Table of Contents

# 材料指南

装修主材、辅材清单，品牌推荐与鉴别方法。

## 目录

- 概述 — 装修材料基础知识

- 主材清单 — 瓷砖、地板、门、橱柜等

- 辅材清单 — 水泥、沙子、电线、水管等

- 品牌推荐 — 各品类口碑品牌

- 材料鉴别 — 真假辨别与选购技巧

# 胶水与粘合剂指南 (Adhesive & Sealant Guide)

## 1. Overview of Adhesive Types Used in Renovation

| Adhesive Type | Chinese Name | Primary Use | Base Material | Cure Mechanism |
| --- | --- | --- | --- | --- |
| Glass Glue / Silicone Sealant | 玻璃胶 | Sealing windows, bathrooms, kitchens | Silicone | Moisture cure |
| Structural Adhesive | 结构胶 | Load-bearing bonds,幕墙 (curtain wall) | Epoxy / Polyurethane / MS Polymer | Chemical cure |
| Tile Adhesive | 瓷砖胶/瓷砖粘结剂 | Bonding tiles to walls/floors | Cement + polymer modified | Water evaporation + hydration |
| Floor Adhesive | 地板胶 | Wood flooring, LVT, rubber flooring | Polyurethane / Acrylic | Solvent evaporation / moisture cure |
| Wood Glue | 木工胶/白乳胶 | Wood joints, cabinetry, trim | PVA (Polyvinyl Acetate) | Water evaporation |
| Polyurethane Foam | 发泡胶/PU发泡剂 | Gap filling, insulation, window sealing | Polyurethane | Moisture cure (expanding) |
| Contact Adhesive | 万能胶 | Laminate, veneer, rubber flooring | Neoprene / Polychloroprene | Solvent evaporation |
| Epoxy Adhesive | 环氧树脂胶 | Metal, stone, structural repair | Two-part epoxy | Chemical reaction (A+B mix) |
| MS Polymer Sealant | MS改性硅烷胶 | General sealing, replacing silicone | Modified silane | Moisture cure |
| Tile Grout (Epoxy) | 环氧美缝剂 | Tile joint filling (bathroom, kitchen) | Epoxy resin | Chemical cure |

## 2. Glass Glue / Silicone Sealant (玻璃胶)

### Types

| Type | Characteristics | Best For | Avoid |
| --- | --- | --- | --- |
| Acidic (酸性) | Strong smell (vinegar), fast cure, strong bond | Glass, mirrors, smooth non-porous surfaces | Marble, cement, metal (corrosive), mirrors with silver backing |
| Neutral (中性) | No odor, slower cure, safe for most materials | General sealing, bathroom, kitchen, stone, metal | None (universal use) |
| Anti-mold (防霉型) | Contains fungicide, neutral or acidic | Bathroom, kitchen, areas with persistent moisture | Food contact surfaces |
| Weather-resistant (耐候型) | UV stable, wide temperature range | Exterior windows, facade sealing | Interior decorative work |

### Application Checklist

- Clean surfaces thoroughly — remove dust, oil, old sealant residue

- Use masking tape on both sides for clean bead lines

- Apply at 5–40°C; cold temperatures slow curing

- Tool the bead within 5 minutes of application

- Remove masking tape immediately after tooling

- Allow 24 hours full cure before exposing to water

- Do NOT paint over silicone (use MS polymer if painting is needed)

### Common Brands

| Brand | Product Line | Notes |
| --- | --- | --- |
| GE (Momentive) | Silicone I / II | Industry standard, reliable |
| Dow (Dow Corning) | 791, 795 | Excellent for construction |
| Wacker (瓦克) | GM, GN | German quality, good anti-mold |
| Sika (西卡) | Sikasil | Strong in structural applications |
| Bai Yun (白云) | Chinese domestic | Cost-effective, good availability |

## 3. Structural Adhesive (结构胶)

### Applications in Renovation

- Bonding stone countertops to cabinets

- Curtain wall panel installation

- Stair nosing and tread bonding

- Heavy mirror mounting (frameless)

- Metal-to-concrete connections

- Glass railing installation

### Types by Chemistry

| Chemistry | Strength | Cure Time | Temperature Range | Best For |
| --- | --- | --- | --- | --- |
| Epoxy | Very high | 5 min – 24 hrs (depends on formula) | -40 to 120°C | Structural stone, metal bonding |
| Polyurethane (PU) | High | 4–24 hrs | -40 to 90°C | Flexible bonds, dissimilar materials |
| MS Polymer | High | 24 hrs (surface cure 30 min) | -40 to 100°C | All-purpose structural, paintable |
| Silicone (structural grade) | Moderate–High | 24 hrs | -50 to 200°C | Glass curtain walls, high-temp areas |

### Selection Guide

| Scenario | Recommended Type | Key Property |
| --- | --- | --- |
| Stone countertop bonding | Epoxy (two-part) | High shear strength, gap filling |
| Glass railing to floor | Structural silicone | UV stable, transparent |
| Metal bracket to concrete | PU structural adhesive | Flexibility, vibration resistance |
| Frameless mirror mounting | MS polymer | Safe for mirror backing, strong |
| Outdoor structural glazing | Structural silicone (ASTM C1184) | Weather resistance |

## 4. Tile Adhesive (瓷砖胶 / 瓷砖粘结剂)

### Classification by Performance Grade

| Grade | Bond Strength | Tile Size Supported | Wall or Floor | Notes |
| --- | --- | --- | --- | --- |
| C0 (Basic) | ≥ 0.5 MPa | Up to 200 x 200mm | Floor only | Basic cement-based, budget |
| C1 (Standard) | ≥ 0.5 MPa (improved) | Up to 400 x 400mm | Wall and floor | Most common for residential |
| C2 (Enhanced) | ≥ 1.0 MPa | Large format (600 x 1200mm+) | Wall and floor | Polymer-modified, for heavy tiles |
| S1 (Flexible) | C2 + ≥ 2.5mm deformation | Large format on flexible substrates | Wall and floor | For underfloor heating, wood substrates |
| S2 (Highly Flexible) | C2 + ≥ 5mm deformation | Very large format, exterior | All | For extreme movement areas |

### C1 vs Traditional Cement Mortar

| Feature | Tile Adhesive (C1) | Cement Mortar |
| --- | --- | --- |
| Bond Strength | 0.5+ MPa | 0.2–0.3 MPa |
| Application Thickness | 3–8mm (thin-bed) | 15–30mm (thick-bed) |
| Material Consumption | 4–6 kg/m² | 15–25 kg/m² |
| Slump Resistance | Excellent (no sagging on walls) | Poor (tiles slide on walls) |
| Water Retention | High (no pre-soaking tiles needed) | Low (tiles must be soaked) |
| Workability | Mix with water only | Requires sand mixing, skill-dependent |

### Application Checklist

- Select grade based on tile size and location (wall vs floor)

- Substrate must be solid, clean, and level (±3mm / 2m)

- Mix to a smooth, lump-free paste; let rest 5 minutes, remix

- Apply with correct notch trowel size:

  - Small tiles (up to 200mm): 6mm notch

  - Medium tiles (200–400mm): 8mm notch

  - Large tiles (400mm+): 10mm notch

- Use double-buttering (apply adhesive to both substrate and tile back) for tiles larger than 400mm

- Press firmly and shift slightly to collapse ridges

- Open time: install within 20 minutes of spreading adhesive

- Do not add extra cement or sand to pre-mixed tile adhesive

### Brand Recommendations

| Brand | Notes |
| --- | --- |
| Mapei (马贝) | Full range C0–S2, excellent quality |
| Davco (德高) | Popular in China, good C1/C2 range |
| Sika (西卡) | SikaCeram line, reliable |
| Oriental Yuhong (东方雨虹) | Domestic leader, cost-effective |
| Bostik (波士胶) | French brand, strong large-format line |

## 5. Floor Adhesive (地板胶)

### Types by Flooring Material

| Flooring Type | Recommended Adhesive | Key Properties |
| --- | --- | --- |
| Solid wood | PU adhesive or elastic MS polymer | Flexible, moisture-tolerant |
| Engineered wood | Solvent-free acrylic or silane-based | Low VOC, fast set |
| LVT / SPC | Pressure-sensitive acrylic | Re-positionable, water-resistant |
| Rubber flooring | Contact adhesive or water-based dispersion | Strong bond, flexible |
| Carpet | Pressure-sensitive or hot-melt | Releasable (for carpet tiles) |

### VOC Considerations

| Adhesive Type | Typical VOC Level | Ventilation Required |
| --- | --- | --- |
| Solvent-based contact adhesive | High (200–600 g/L) | Yes, 48+ hours |
| Water-based acrylic | Low (< 50 g/L) | Minimal |
| MS Polymer | Very Low (< 10 g/L) | Minimal |
| Solvent-free PU | Low (< 30 g/L) | 24 hours |

Rule: Always choose water-based or solvent-free floor adhesives for occupied residential spaces. Verify VOC compliance with GB 18583 (Chinese indoor adhesive standard) or equivalent.

## 6. Wood Glue / PVA Adhesive (木工胶)

### Types

| Type | Color When Dry | Water Resistance | Set Time | Use |
| --- | --- | --- | --- | --- |
| White PVA (白乳胶) | Transparent | None (interior only) | 30 min clamp, 24 hr cure | Indoor furniture, cabinetry |
| Yellow PVA (黄胶) | Amber | Moderate (D2) | 30 min clamp | Interior wood, trim |
| Cross-linked PVA (D3/D4) | Transparent/amber | High (exterior grade) | 1–2 hr clamp | Outdoor furniture, boats |
| Urea-Formaldehyde (脲醛胶) | Hard, brittle | Good | Fast (with catalyst) | Plywood, particleboard manufacturing |
| EVA Hot Melt (热熔胶) | Transparent | None | Instant | Edge banding, quick assembly |

### PVA Application Tips

- Apply thin, even coat to ONE surface only

- Clamp for minimum 30 minutes at 20°C

- Full cure takes 24 hours before sanding or finishing

- Clean excess with damp cloth before drying

- Shelf life: 12 months unopened; discard if lumpy or separated

### VOC Note on Wood Glues

- Standard PVA: Very low VOC, safe for indoor use

- Urea-formaldehyde: Releases formaldehyde; avoid in residential applications where possible; use E0/E1 graded products

- Polyurethane wood glue: Moderate VOC during cure, inert after cure

## 7. Polyurethane Foam Sealant (发泡胶 / PU发泡剂)

### Types

| Type | Expansion | Best For |
| --- | --- | --- |
| High-expansion | Expands 2–3x volume | Large gaps (> 20mm), void filling |
| Low-expansion | Expands 1.2–1.5x | Window/door frames (prevents bowing) |
| Gun-grade | Precise application, controlled expansion | Professional work, narrow gaps |
| Straw-grade | DIY use, disposable | One-off small jobs |

### Application Checklist

- Choose low-expansion foam for window/door frames to avoid distortion

- Fill gap only 1/3 to 1/2 full (foam expands)

- Dampen substrate slightly for better adhesion

- Trim excess after full cure (typically 2–4 hours)

- Cut surface must be sealed with silicone or paint (UV degrades foam)

- Never use in gaps narrower than 5mm or wider than 80mm without multiple passes

## 8. VOC and Health Considerations

### VOC Levels by Adhesive Category

| Category | VOC Range | Indoor Air Quality Impact | Recommendations |
| --- | --- | --- | --- |
| Silicone sealant | Very low (post-cure) | Minimal after 24 hrs | Choose neutral, anti-mold for bathrooms |
| Epoxy | Low–Moderate | Moderate during mixing/cure | Ventilate during use; inert after cure |
| Solvent-based contact adhesive | High | Significant for 48–72 hrs | Avoid in residential; use water-based alternative |
| Water-based PVA/acetate | Very low | Negligible | Safe for all indoor use |
| PU foam (uncured) | Moderate | Moderate for 4–8 hrs | Ventilate; inert after trim |
| Tile adhesive (cement-based) | None | None | Dust hazard during mixing — wear mask |
| MS Polymer | Very low | Negligible | Best all-around low-VOC option |

### Key Standards

- GB 18583-2008: Chinese national standard for indoor decorative adhesives (VOC limits)

- GREENGUARD Gold: Low emission certification for indoor air quality

- EC1 Plus (EMICODE): European standard, lowest emission class

- A+ (French VOC label): Highest indoor air quality rating

### Practical VOC Reduction Tips

- Choose products labeled E0, GREENGUARD, or EC1 Plus

- Ventilate continuously during and after adhesive application

- Allow 72-hour cure period before occupying renovated space

- Use air purifiers with activated carbon during curing

- Avoid mixing different adhesive brands on the same job

- Store adhesives sealed and in cool conditions to prevent premature off-gassing

## 9. Quick Selection Matrix

| Task | Best Adhesive | Alternative | Notes |
| --- | --- | --- | --- |
| Seal bathroom sink to counter | Neutral anti-mold silicone | MS polymer | Anti-mold grade essential |
| Bond tile to wall | C1 or C2 tile adhesive | — | Use notch trowel |
| Fix wood trim | White PVA (D2) | Construction adhesive | Clamp 30 min |
| Mount frameless mirror | MS polymer | Structural silicone | Must be mirror-safe |
| Seal window perimeter | Low-expansion PU foam | — | Trim and seal surface |
| Bond stone countertop | Two-part epoxy | — | Structural strength required |
| Edge banding | EVA hot melt | Contact adhesive | Use edge banding machine |
| Fill gap between cabinet and wall | Neutral silicone | MS polymer | Paintable if MS |
| Install LVT flooring | Pressure-sensitive acrylic | — | Follow manufacturer TDS |
| Outdoor wood repair | D3/D4 PVA or PU wood glue | Epoxy | Must be waterproof |

# 家电尺寸与预留指南 (Appliance Sizing & Pre-planning Guide)

## 概述

家电的尺寸预留是装修前期规划的重要环节。尺寸不当会导致无法安装、散热不良、使用不便等问题。本指南汇总了常见家电的标准尺寸、安装间隙要求及水电预留要点，帮助在装修设计阶段做出正确的预留决策。

## 一、厨房电器

### 1.1 冰箱

| 类型 | 宽度(mm) | 深度(mm) | 高度(mm) | 容量范围 | 适用家庭 |
| --- | --- | --- | --- | --- | --- |
| 单门 | 500-550 | 550-600 | 850-900 | 100-150L | 单身/小公寓 |
| 双门 | 550-600 | 600-650 | 1400-1700 | 200-300L | 2-3人 |
| 三门 | 550-600 | 600-650 | 1700-1800 | 250-350L | 3-4人 |
| 对开门 | 850-950 | 650-750 | 1700-1800 | 500-650L | 4-6人 |
| 十字对开门 | 750-850 | 650-750 | 1700-1800 | 400-550L | 4-6人 |
| 嵌入式 | 540-560 | 545-550 | 1770-1780 | 250-350L | 定制橱柜 |

#### 预留要点

- 散热间隙：两侧各留50-100mm，顶部留50mm，背部留50mm

- 嵌入式冰箱：必须使用底部散热或前置散热型号，两侧间隙可缩小至5-10mm

- 插座：10A三孔插座，距地300-500mm（冰箱后方或侧面）

- 开门空间：确认门开启角度不被橱柜或墙体阻挡（通常需≥90°才能拉出抽屉）

- 柜体深度：橱柜深度≥冰箱深度+50mm

### 1.2 洗碗机

| 类型 | 宽度(mm) | 深度(mm) | 高度(mm) | 套数 |
| --- | --- | --- | --- | --- |
| 台式/ countertop | 550 | 500 | 450 | 4-6套 |
| 嵌入式（标准） | 598 | 550 | 775 | 12-14套 |
| 嵌入式（紧凑型） | 448 | 550 | 815 | 8-10套 |
| 水槽式 | 550-600 | 500 | - | 4-6套 |

#### 预留要点

- 柜体尺寸：宽600mm×深550mm×高820mm（标准嵌入式）

- 进出水：进水口（角阀）和排水口留在相邻柜体内

- 插座：10A三孔插座，安装在相邻柜体（不可留在机器正后方）

- 柜门匹配：确认是否使用橱柜同色门板（全嵌式）或自带门板（半嵌式）

- 台面开孔：水槽式洗碗机需按型号开孔，尺寸差异大

### 1.3 烤箱/蒸烤箱

| 类型 | 宽度(mm) | 深度(mm) | 高度(mm) |
| --- | --- | --- | --- |
| 嵌入式（60cm标准） | 595 | 550-570 | 595 |
| 嵌入式（45cm紧凑） | 595 | 550-570 | 455 |
| 嵌入式（双腔） | 595 | 550-570 | 890 |

#### 预留要点

- 柜体尺寸：宽600mm×深560mm×高600mm（单腔标准）

- 散热：背部或底部预留散热空间，不得封闭通风口

- 插座：16A三孔插座（功率通常>3000W），安装在相邻柜体

- 台面高度：嵌入式烤箱建议安装在900-1000mm高度，方便操作

- 隔热：周边柜体板材需耐温≥80℃

### 1.4 烟机灶具

| 电器 | 宽度(mm) | 深度(mm) | 高度(mm) | 备注 |
| --- | --- | --- | --- | --- |
| 侧吸烟机 | 750-900 | 350-450 | 600-800 | 安装高度距灶台350-400mm |
| 顶吸烟机 | 750-900 | 500-550 | 500-700 | 安装高度距灶台650-700mm |
| 集成灶 | 750-900 | 600 | 800-850 | 集成烟机+灶具 |
| 燃气灶 | 600-750 | 350-450 | 150-200 | 开孔尺寸需按型号 |

#### 预留要点

- 烟道：直径160-180mm烟管，止逆阀安装在烟道口

- 插座：烟机插座（10A）在吊顶内，距顶300mm；灶具插座（如需电）在橱柜内

- 燃气：燃气表、燃气阀门预留位置（通常在水槽下方柜体）

- 台面开孔：燃气灶开孔尺寸按产品说明书，通常宽×深=650×350mm

## 二、卫浴电器

### 2.1 热水器

| 类型 | 宽度(mm) | 深度(mm) | 高度(mm) | 容量 | 安装位置 |
| --- | --- | --- | --- | --- | --- |
| 电热水器（立式） | 400-450 | 400-450 | 700-900 | 50-80L | 卫生间墙面 |
| 电热水器（卧式） | 700-900 | 350-450 | 350-450 | 50-80L | 卫生间顶部 |
| 燃气热水器 | 330-380 | 150-200 | 500-550 | - | 厨房/阳台 |
| 空气能热水器 | 500-600 | 500-600 | 1500-1800 | 150-200L | 阳台/设备间 |

#### 预留要点

- 电热水器插座：16A三孔插座，距地1800-2000mm

- 燃气热水器：燃气管道、排烟管（直径60mm）预留

- 承重：电热水器满水重量>100kg，必须安装在承重墙

- 进出水口：冷热水角阀，距地1400-1500mm

- 排水：安全阀排水管引至地漏

### 2.2 洗衣机/烘干机

| 类型 | 宽度(mm) | 深度(mm) | 高度(mm) | 容量 |
| --- | --- | --- | --- | --- |
| 滚筒洗衣机 | 595-600 | 500-600 | 850 | 7-10kg |
| 波轮洗衣机 | 520-550 | 550-600 | 900-950 | 6-8kg |
| 热泵烘干机 | 595-600 | 600-660 | 850 | 7-9kg |
| 洗烘一体 | 595-600 | 600-650 | 850 | 7-10kg/4-7kg |
| 洗烘套装（叠放） | 595-600 | 600-660 | 1700 | - |

#### 预留要点

- 柜体尺寸：宽650mm×深650mm×高900mm（单台）

- 叠放：使用连接件固定，总高度约1750mm

- 进水：洗衣机龙头（专用角阀），距地500-600mm

- 排水：地漏或专用排水管，距地100-200mm

- 插座：10A三孔插座，距地1200-1400mm（不可留在机器正后方）

- 烘干机排气：冷凝式无需排气，热泵式无需排气

## 三、客厅/卧室电器

### 3.1 空调

| 类型 | 室内机尺寸(mm) | 室外机尺寸(mm) | 匹数 | 适用面积 |
| --- | --- | --- | --- | --- |
| 挂机 | 800-900×280-320×200-250 | 700-800×540-580×250-320 | 1-1.5P | 10-20㎡ |
| 柜机 | 500-550×350-400×1700-1800 | 800-900×600-700×320-400 | 2-3P | 20-40㎡ |
| 风管机（单联） | 按型号定制 | 同挂机 | 1-3P | 按需 |
| 中央空调（多联） | 按型号定制 | 900-1200×700-800×350-450 | 4-8P | 全屋 |

#### 预留要点

- 挂机插座：16A三孔插座，距地2000-2200mm

- 柜机插座：16A或20A三孔插座，距地300mm

- 空调孔：直径50-75mm，内高外低（防雨水倒灌）

- 冷凝水管：PVC25管，坡度≥1%

- 中央空调：吊顶内预留检修口（≥400×400mm）

- 室外机位：确认尺寸、散热空间（前后≥200mm，顶部≥500mm）

### 3.2 电视

| 尺寸 | 宽度(mm) | 高度(mm) | 厚度(mm) | 建议观看距离 |
| --- | --- | --- | --- | --- |
| 55英寸 | 1230 | 710 | 60-80 | 2.2-2.8m |
| 65英寸 | 1450 | 840 | 60-80 | 2.6-3.2m |
| 75英寸 | 1670 | 960 | 60-80 | 3.0-3.8m |
| 85英寸 | 1900 | 1100 | 60-80 | 3.4-4.2m |

#### 预留要点

- 插座：至少4个五孔插座（电视、机顶盒、路由器、音响），距地350-400mm或隐藏在电视后方

- 网线：Cat6或Cat6a网线，距地350-400mm

- HDMI管：预埋φ50 PVC管（隐藏走线），两端出线口

- 电视柜：深度≥400mm（如需放置设备）

- 壁挂：确认墙体承重，使用膨胀螺栓或预埋加固件

## 四、水电预留汇总表

### 4.1 厨房电器预留

| 电器 | 插座规格 | 插座高度 | 插座位置 | 备注 |
| --- | --- | --- | --- | --- |
| 冰箱 | 10A三孔 | 300-500mm | 侧面/旁边柜体 | 单独回路 |
| 洗碗机 | 10A三孔 | 500-600mm | 旁边柜体 | 不可在正后方 |
| 烤箱 | 16A三孔 | 500-600mm | 旁边柜体 | ≥3000W |
| 烟机 | 10A三孔 | 2200mm | 烟机上方吊顶内 | - |
| 燃气灶 | 10A三孔 | 500mm | 下方柜体（如需） | 仅电子点火需要 |
| 净水器 | 10A三孔 | 500mm | 水槽下方柜体 | 带RO反渗透需要 |
| 垃圾处理器 | 10A三孔 | 500mm | 水槽下方柜体 | 带开关插座 |
| 微波炉 | 10A三孔 | 1400mm | 台面附近 | 嵌入式需提前规划 |

### 4.2 卫浴电器预留

| 电器 | 插座规格 | 插座高度 | 插座位置 | 备注 |
| --- | --- | --- | --- | --- |
| 电热水器 | 16A三孔 | 1800-2000mm | 热水器旁 | 带防溅盒 |
| 洗衣机 | 10A三孔 | 1200-1400mm | 机器侧上方 | 带防溅盒 |
| 烘干机 | 10A三孔 | 1200-1400mm | 机器侧上方 | - |
| 智能马桶 | 10A三孔 | 300-400mm | 马桶侧方 | 带防溅盒 |
| 电热毛巾架 | 10A三孔 | 1200-1400mm | 毛巾架旁 | - |
| 镜柜灯/除雾 | 10A两孔 | 1800-2000mm | 镜柜内/后方 | - |

## 五、常见预留错误

| 错误 | 后果 | 正确做法 |
| --- | --- | --- |
| 插座留在电器正后方 | 电器无法贴墙，突出柜体 | 插座留在侧面或相邻柜体 |
| 冰箱预留宽度不够 | 门无法打开90°，抽屉拉不出 | 预留宽度=冰箱宽度+两侧各100mm |
| 未预留空调孔 | 明管穿墙，影响美观 | 装修前期打孔，内高外低 |
| 洗碗机进出水留在正后方 | 机器无法推入 | 留在相邻柜体 |
| 电视背景墙插座外露 | 电线凌乱 | 使用隐藏式插座或穿管隐藏 |
| 未考虑烘干机 | 后期无法加装 | 提前预留空间和插座 |
| 空调外机位尺寸不足 | 外机无法安装或散热不良 | 按外机尺寸+散热空间预留 |

## 六、预规划检查清单

### 装修前确认

- 列出所有需要安装的电器清单

- 确认每个电器的具体型号和尺寸

- 绘制电器布置图，标注尺寸

- 确认每个电器的水电需求（插座、进水、排水、燃气）

- 确认散热空间要求

- 确认开门/开盖空间要求

- 与设计师/施工方交底确认

### 施工中确认

- 水电交底时逐一核对电器预留点位

- 水电验收时检查每个预留点位

- 橱柜设计时确认电器尺寸和间隙

- 吊顶施工前确认烟机/空调管道走向

### 安装前确认

- 电器到货后复测实际尺寸

- 确认预留空间满足安装要求

- 确认水电接口与电器匹配

- 预约安装时间与装修进度协调

# 装修辅材清单详解

## 水泥砂浆

| 材料 | 用途 | 估算量 |
| --- | --- | --- |
| 水泥 | 砌筑、找平 | 10-20袋 |
| 沙子 | 砂浆、找平 | 2-5方 |
| 石子 | 混凝土 | 按需要 |

## 水电材料

| 材料 | 规格 | 估算量 |
| --- | --- | --- |
| PPR管 | 4分/6分 | 50-100m |
| PVC管 | 16/20mm | 100-200m |
| 电线 | 1.5/2.5/4mm² | 200-500m |
| 底盒 | 86型 | 30-60个 |

## 防水材料

| 材料 | 用途 | 估算量 |
| --- | --- | --- |
| 防水涂料 | 厨卫防水 | 按面积计算 |

## 吊顶材料

| 材料 | 用途 | 估算量 |
| --- | --- | --- |
| 轻钢龙骨 | 吊顶骨架 | 按面积计算 |
| 石膏板 | 吊顶面板 | 按面积计算 |

## 其他辅料

| 材料 | 用途 |
| --- | --- |
| 腻子 | 墙面找平 |
| 界面剂 | 基层处理 |
| 填缝剂 | 瓷砖填缝 |
| 发泡胶 | 门窗填缝 |
| 玻璃胶 | 密封 |

# 辅材清单

装修辅材虽然单价不高，但种类多、用量大，是半包中装修公司提供的部分。

## 基础建材

- 水泥（325#、425#）

- 沙子（中沙、粗沙）

- 红砖/轻体砖

- 石膏粉

- 腻子粉

## 水电材料

- PPR 水管及管件

- PVC 电线管及管件

- 电线（1.5mm²、2.5mm²、4mm²）

- 底盒

- 弯头、三通等管件

## 防水材料

- 聚氨酯防水涂料

- JS 防水涂料

- 堵漏王

## 五金辅料

- 钉子（钢钉、水泥钉、自攻螺丝）

- 胶带（生料带、绝缘胶布）

- 管卡、吊杆

- 龙骨（轻钢龙骨、木龙骨）

# 卫浴选购指南

## 马桶选择

### 类型对比

| 类型 | 价格（元） | 优点 | 缺点 |
| --- | --- | --- | --- |
| 连体马桶 | 800-2000 | 便宜、易清洁 | 造型一般 |
| 分体马桶 | 500-1500 | 最便宜 | 接缝易脏 |
| 壁挂马桶 | 2000-6000 | 美观、易清洁 | 价格高、安装复杂 |
| 智能马桶 | 2000-10000 | 功能多、舒适 | 价格高、需预留插座 |

### 选购要点

- 冲水方式：虹吸式 > 直冲式（噪音小、防臭）

- 坑距：300mm 或 400mm，购买前确认

- 水件：优质水件决定使用寿命

- 釉面：全管道施釉，不易堵塞

## 花洒选择

### 类型

| 类型 | 价格（元） | 特点 |
| --- | --- | --- |
| 手持花洒 | 200-800 | 灵活方便 |
| 顶喷花洒 | 500-2000 | 淋浴体验好 |
| 恒温花洒 | 800-3000 | 水温稳定 |
| 空气注入花洒 | 500-2000 | 节水、舒适 |

### 选购要点

- 阀芯：陶瓷阀芯最耐用

- 材质：铜质龙头 > 不锈钢 > 锌合金

- 表面处理：电镀铬最耐用

- 品牌推荐：汉斯格雅、高仪、科勒、TOTO、九牧、箭牌

## 浴室柜选择

### 类型

| 类型 | 特点 | 适用场景 |
| --- | --- | --- |
| 落地式 | 储物空间大 | 大卫生间 |
| 壁挂式 | 易清洁、防潮 | 小卫生间 |

### 选购要点

- 材质：多层实木 > PVC > 密度板

- 台面：陶瓷一体 > 岩板 > 人造石

- 防潮：底部防水处理

- 五金：不锈钢铰链和滑轨

## 淋浴房选择

### 类型

| 类型 | 价格（元/㎡） | 适用场景 |
| --- | --- | --- |
| 一字型 | 500-1500 | 靠墙安装 |
| 弧型 | 600-1800 | 角落安装 |
| 钻石型 | 700-2000 | 角落安装 |
| 浴缸隔断 | 500-1500 | 浴缸上方 |

### 选购要点

- 玻璃：必须是钢化玻璃，有 3C 认证

- 厚度：≥6mm

- 五金：不锈钢或铝合金

- 密封条：磁吸密封条密封性好

# 装修材料品牌推荐

## 瓷砖品牌

| 档次 | 品牌 | 特点 |
| --- | --- | --- |
| 高端 | 马可波罗、诺贝尔 | 品质好、价格高 |
| 中端 | 东鹏、冠珠 | 性价比高 |
| 经济 | 地方品牌 | 价格便宜 |

## 地板品牌

| 档次 | 品牌 | 特点 |
| --- | --- | --- |
| 高端 | 大自然、圣象 | 品质好 |
| 中端 | 生活家、德尔 | 性价比高 |
| 经济 | 地方品牌 | 价格便宜 |

## 涂料品牌

| 档次 | 品牌 | 特点 |
| --- | --- | --- |
| 高端 | 芬琳、都芳 | 环保好 |
| 中端 | 多乐士、立邦 | 性价比高 |
| 经济 | 三棵树、嘉宝莉 | 价格便宜 |

## 卫浴品牌

| 档次 | 品牌 | 特点 |
| --- | --- | --- |
| 高端 | 科勒、TOTO | 品质好 |
| 中端 | 箭牌、九牧 | 性价比高 |
| 经济 | 恒洁、惠达 | 价格便宜 |

## 门窗品牌

| 档次 | 品牌 | 特点 |
| --- | --- | --- |
| 高端 | 盼盼、美心 | 品质好 |
| 中端 | 步阳、星月神 | 性价比高 |
| 经济 | 地方品牌 | 价格便宜 |

# 品牌推荐

## 瓷砖品牌

- 马可波罗、东鹏、诺贝尔、冠珠、蒙娜丽莎

## 地板品牌

- 大自然、圣象、生活家、德尔

## 涂料品牌

- 多乐士、立邦、三棵树、嘉宝莉

## 水管品牌

- 伟星、日丰、金牛、联塑

## 电线品牌

- 远东、熊猫、金杯、正泰

## 防水品牌

- 东方雨虹、德高、西卡、卓宝

# 橱柜选购详解

## 橱柜组成

- 柜体

- 门板

- 台面

- 五金

- 拉篮

- 功能件

## 柜体材料

| 材料 | 价格 | 优点 | 缺点 |
| --- | --- | --- | --- |
| 颗粒板 | 中 | 稳定性好 | 怕潮 |
| 多层板 | 中高 | 防潮好 | 价格高 |
| 生态板 | 高 | 环保 | 贵 |

## 门板材料

| 材料 | 价格 | 特点 |
| --- | --- | --- |
| 双饰面板 | 低 | 性价比高 |
| PET | 中 | 易清洁 |
| 实木 | 高 | 质感好 |
| 烤漆 | 中高 | 光泽好 |
| 模压 | 中 | 可造型 |

## 台面选择

| 材料 | 价格 | 优点 | 缺点 |
| --- | --- | --- | --- |
| 石英石 | 中 | 硬度高 | 接缝可见 |
| 岩板 | 高 | 抗菌美观 | 贵 |
| 不锈钢 | 中 | 耐用 | 易刮花 |
| 人造石 | 中 | 可一体成型 | 易渗色 |

## 五金配置

- 铰链：带缓冲

- 滑轨：三节轨

- 拉篮：调味拉篮、碗碟拉篮

- 气撑：上翻门用

## 计价方式

### 延米计价

总价 = 延米数 × 延米单价

### 柜体计价

总价 = 各柜体价格 + 台面 + 五金

## 验收要点

- 柜体牢固

- 门板平整

- 五金顺畅

- 台面无缝

- 尺寸准确

# 装修主材采购清单

## 瓷砖类

- 客厅地砖

- 卧室地砖（可选地板）

- 厨卫墙砖

- 厨卫地砖

- 阳台砖

## 地板类

- 地板

- 踢脚线

- 防潮垫

## 门类

- 入户门

- 卧室门

- 卫生间门

- 厨房门

## 橱柜

- 厨房地柜

- 厨房吊柜

- 台面

## 卫浴

- 马桶

- 花洒

- 浴室柜

- 淋浴房

## 其他

- 窗户

- 吊顶材料

- 涂料

- 开关插座

- 灯具

## 采购时间线

| 材料 | 采购时间 | 进场时间 |
| --- | --- | --- |
| 窗户 | 拆改前 | 拆改阶段 |
| 瓷砖 | 泥瓦前 | 泥瓦阶段 |
| 地板 | 油漆前 | 安装阶段 |
| 门 | 油漆前 | 安装阶段 |
| 橱柜 | 泥瓦前 | 安装阶段 |
| 卫浴 | 泥瓦前 | 安装阶段 |

# 装修材料对比

## 瓷砖对比

| 类型 | 优点 | 缺点 | 价格 |
| --- | --- | --- | --- |
| 抛光砖 | 光亮、耐磨 | 防滑差 | 中 |
| 釉面砖 | 花色多 | 易碎 | 中高 |
| 通体砖 | 耐磨 | 花色少 | 中 |

## 地板对比

| 类型 | 优点 | 缺点 | 价格 |
| --- | --- | --- | --- |
| 实木 | 环保、脚感好 | 贵、需保养 | 高 |
| 复合 | 稳定、性价比 | 胶水粘合 | 中 |
| 强化 | 耐磨、便宜 | 脚感硬 | 低 |

## 涂料对比

| 类型 | 优点 | 缺点 | 价格 |
| --- | --- | --- | --- |
| 乳胶漆 | 环保、易施工 | 质感单一 | 中 |
| 壁纸 | 花色多 | 寿命短 | 中 |
| 硅藻泥 | 调湿 | 贵 | 高 |

# 台面材料选购指南 (Countertop Materials Guide)

## 1. Countertop Material Overview

| Material | Chinese Name | Cost Range (per linear meter) | Durability | Maintenance | Heat Resistance | Stain Resistance |
| --- | --- | --- | --- | --- | --- | --- |
| Quartz (Engineered Stone) | 石英石台面 | ¥400–1500 | Excellent | Low | Good (not excellent) | Excellent |
| Granite (Natural Stone) | 花岗岩台面 | ¥600–2000+ | Excellent | Moderate | Excellent | Good (when sealed) |
| Marble (Natural Stone) | 大理石台面 | ¥800–3000+ | Moderate | High | Good | Poor (etches easily) |
| Stainless Steel | 不锈钢台面 | ¥500–1200 | Excellent | Low | Excellent | Excellent |
| Solid Surface (Acrylic) | 人造石/亚克力台面 | ¥400–1200 | Good | Low | Poor | Good |
| Laminate | 防火板/层压板台面 | ¥150–500 | Fair | Low | Poor | Good |
| Sintered Stone | 岩板台面 | ¥800–2500+ | Excellent | Low | Excellent | Excellent |
| Concrete | 混凝土台面 | ¥600–1500 | Good | High | Excellent | Good (when sealed) |
| Wood / Butcher Block | 实木台面 | ¥400–1000 | Fair | High | Moderate | Poor |

## 2. Quartz Countertop (石英石台面)

### Composition

- 90–94% crushed natural quartz

- 6–10% polymer resin and pigments

- Manufactured under high pressure and vibration

### Performance Data

| Property | Rating | Notes |
| --- | --- | --- |
| Mohs Hardness | 6–7 | Harder than granite in some cases |
| Water Absorption | 0.02% | Virtually non-porous |
| Flexural Strength | 20–40 MPa | Strong, but can chip at edges |
| Heat Resistance | Up to 150°C | Resin binder can discolor above this |
| Stain Resistance | Excellent | No sealing required |
| UV Stability | Moderate | Prolonged direct sunlight may cause yellowing |

### Thickness Options

| Thickness | Best For | Notes |
| --- | --- | --- |
| 15mm | Budget kitchens, light use | Requires plywood subtop |
| 20mm | Standard residential | Most common, no subtop needed |
| 30mm | Premium / commercial | Heavy, requires sturdy cabinet support |

### Quality Checklist — What to Look For

- Quartz content 90%+ (check product specification)

- Brand-marked slab (avoid unbranded “white label” quartz)

- Uniform pattern with no visible resin pooling

- Edge polish is even with no chip marks

- Back of slab has manufacturer logo and batch number

- Request material test certificate (especially for formaldehyde and heavy metals)

- Minimum 10-year warranty from manufacturer

### Common Brands

| Brand | Origin | Price Tier | Notes |
| --- | --- | --- | --- |
| CaesarsStone | Israel | Premium | Original engineered quartz |
| Silestone (Cosentino) | Spain | Premium | Wide color range, antimicrobial |
| HanStone (韩石) | Korea | Mid–High | Good value |
| Zhongxun (中讯) | China | Mid | Largest domestic producer |
| Opal (欧派配套) | China | Mid | Common in custom cabinet packages |

## 3. Granite Countertop (花岗岩台面)

### Characteristics

- Natural stone, each slab is unique

- Mined in blocks, cut and polished

- Requires periodic sealing

### Common Granite Types

| Type | Origin | Color | Typical Use | Cost |
| --- | --- | --- | --- | --- |
| Black Galaxy | India | Black with gold flecks | Kitchen, vanity | High |
| Absolute Black | India | Solid black | Modern kitchens | High |
| G603 / Sesame White | China | White/gray speckle | Budget natural stone | Low |
| Ubatuba | Brazil | Dark green/black | Traditional kitchens | Mid |
| Santa Cecilia | Brazil | Beige/brown/gold | Warm traditional style | Mid |
| Blue Pearl | Norway | Blue-gray with shimmer | Premium statement | Very High |

### Maintenance Schedule

| Task | Frequency | Method |
| --- | --- | --- |
| Daily cleaning | Daily | Warm water + mild soap |
| Deep clean | Weekly | Stone-specific cleaner |
| Seal application | Every 1–2 years | Penetrating sealer |
| Water test | Every 6 months | Drop water on surface; if it darkens, reseal |
| Professional polish | Every 3–5 years | Stone restoration service |

### Pros and Cons

| Pros | Cons |
| --- | --- |
| Unique natural beauty | Requires sealing |
| Excellent heat resistance (hot pans OK) | Can crack under impact |
| Very durable, lasts decades | Seams may be visible |
| Increases home value | Heavy (requires strong cabinet support) |
| Resistant to scratches | Natural fissures and pits are normal |

## 4. Marble Countertop (大理石台面)

### Characteristics

- Calcium carbonate-based; reacts with acids (etching)

- Prized for veining and elegance

- Best suited for bathrooms, vanity tops, pastry areas (low acid exposure)

### Common Marble Types

| Type | Origin | Appearance | Price |
| --- | --- | --- | --- |
| Carrara | Italy | White with soft gray veins | Mid–High |
| Calacatta | Italy | White with bold gold/gray veins | Very High |
| Statuario | Italy | Pure white with dramatic veining | Premium |
| Emperador Dark | Spain | Dark brown with lighter veins | Mid |
| Cream Marfil | Spain | Cream/beige uniform | Mid |
| Domestic white (国产白大理石) | China | White, varied quality | Low–Mid |

### Care Requirements

- NEVER place acidic substances (lemon, vinegar, wine) directly on marble

- Use coasters and trivets at all times

- Seal upon installation and every 6–12 months

- Clean only with pH-neutral stone cleaner

- Etch marks can be professionally polished out

- Not recommended for primary kitchen countertops in heavy cooking households

## 5. Stainless Steel Countertop (不锈钢台面)

### Specifications

| Property | Value |
| --- | --- |
| Common grade | 304 stainless steel (food grade) |
| Thickness | 1.0–1.5mm (residential); 2.0mm+ (commercial) |
| Surface finish | Brushed (拉丝), mirror (镜面), embossed (压花) |
| Core material | Plywood or particleboard substrate, or hollow |

### Pros and Cons

| Pros | Cons |
| --- | --- |
| 100% hygienic, non-porous | Scratches easily (develops patina) |
| Impervious to heat, water, chemicals | Can dent under impact |
| Seamless fabrication possible | Industrial look (not for all styles) |
| Easy to clean | Shows fingerprints on mirror finish |
| Fireproof | Hollow types sound “tinny” when items placed |
| Long-lasting | Higher-quality (1.5mm+ 304) is expensive |

### Selection Checklist

- Specify 304 grade stainless steel (not 201, which rusts)

- Minimum 1.2mm thickness for residential (1.5mm preferred)

- Brushed finish hides scratches better than mirror

- Verify substrate: plywood core is quieter and more solid than hollow

- Check weld quality on corners — should be smooth, continuous

- Ensure undersink area has water drainage groove

- Edge profile: rolled edge is safer than sharp square edge

## 6. Solid Surface / Acrylic (人造石台面)

### Composition

- Acrylic (PMMA) or polyester resin + mineral fillers

- Can be thermoformed into seamless shapes with integrated sinks

### Performance

| Property | Acrylic-based | Polyester-based |
| --- | --- | --- |
| Durability | Good | Moderate |
| Repairability | Excellent (scratches can be sanded out) | Moderate |
| Heat Resistance | Up to 90°C | Up to 80°C |
| Stain Resistance | Good | Good |
| Seam Visibility | Nearly invisible (color-matched adhesive) | Visible |
| Cost | Moderate | Low |

### Best Applications

- Bathroom vanities (seamless with integrated basin)

- Reception desks and commercial counters

- Kitchen islands with curved profiles

- NOT recommended near cooktops (heat sensitivity)

### Brand Leaders

| Brand | Notes |
| --- | --- |
| Corian (DuPont) | Original solid surface, premium |
| HI-MACS (LG) | Good quality, wide colors |
| Staron (Samsung) | Competitive pricing |
| Domestic brands | Many options; verify acrylic content percentage |

## 7. Sintered Stone (岩板台面)

### What Is It?

- Natural minerals (feldspar, silica) pressed at 1200°C+ and extreme pressure

- Essentially a high-performance porcelain/stone composite

### Performance Comparison vs Quartz

| Property | Sintered Stone | Quartz |
| --- | --- | --- |
| Heat Resistance | Up to 1200°C+ (direct flame OK) | Up to 150°C |
| Scratch Resistance | Mohs 6–7 | Mohs 6–7 |
| Stain Resistance | Excellent (near-zero absorption) | Excellent |
| UV Stability | Excellent (no yellowing) | Moderate (may yellow) |
| Impact Resistance | Moderate (can chip at edges) | Good |
| Fabrication | Requires diamond tools, specialist | Standard stone tools |
| Cost | Higher (¥800–2500/m) | Mid (¥400–1500/m) |
| Thickness | 6mm, 12mm, 20mm | 15mm, 20mm, 30mm |
| Maximum Slab Size | Up to 3600 x 1600mm | Up to 3200 x 1600mm |

### Pros and Cons

| Pros | Cons |
| --- | --- |
| Superior heat resistance | Brittle — can chip or crack on impact |
| UV stable (outdoor OK) | Requires specialist fabricator |
| Near-zero water absorption | Edge profiles limited (hard to shape) |
| Food-safe, antibacterial | Undermount sink installation is tricky |
| Thin profiles (6mm) allow lightweight cabinets | Repair of chips is difficult |

## 8. Laminate Countertop (防火板台面)

### Construction

- Decorative HPL (High-Pressure Laminate) surface

- Particleboard or MDF substrate

- Post-formed or flat edge options

### Pros and Cons

| Pros | Cons |
| --- | --- |
| Most economical option | Not heat resistant (no hot pans) |
| Huge variety of colors/patterns | Water damage at seams and edges |
| Easy DIY installation | Cannot be repaired (must replace) |
| Lightweight | Shorter lifespan (5–15 years) |
| Smooth, easy to clean | Seams are visible |

### Lifespan Expectancy

- Budget laminate: 5–8 years

- Premium (Formica, Wilsonart): 10–15 years

- Failure mode: edge swelling from water ingress, delamination, burn marks

## 9. Detailed Material Comparison

### Heat Resistance Test

| Material | Hot Pot (200°C) Direct Contact | Boiling Water | Oven-to-Counter |
| --- | --- | --- | --- |
| Granite | Safe | Safe | Safe |
| Marble | Risk of thermal shock | Safe | Safe |
| Quartz | Risk of discoloration | Safe | Safe |
| Sintered Stone | Safe | Safe | Safe |
| Stainless Steel | Safe | Safe | Safe |
| Solid Surface | Risk of damage | Safe | Risk of damage |
| Laminate | Will burn/melt | Risk of edge damage | Will damage |
| Wood | Burn marks | Water ring risk | Will scorch |

### Maintenance Effort Scale

| Material | Daily Cleaning | Periodic Treatment | Annual Effort |
| --- | --- | --- | --- |
| Quartz | Wipe with damp cloth | None | Minimal |
| Granite | Wipe with stone cleaner | Seal every 1–2 years | 30 min |
| Marble | Wipe with pH-neutral cleaner | Seal every 6–12 months | 1–2 hours |
| Stainless Steel | Wipe; use stainless cleaner | None | Minimal |
| Solid Surface | Wipe; sand out scratches | None | Minimal |
| Sintered Stone | Wipe with damp cloth | None | Minimal |
| Laminate | Wipe with damp cloth | None | Minimal |
| Wood | Wipe dry immediately | Oil every 3–6 months | 2–3 hours |

### Cost Comparison (Including Installation, per linear meter)

| Material | Budget | Mid-Range | Premium |
| --- | --- | --- | --- |
| Laminate | ¥150–250 | ¥250–400 | ¥400–500 |
| Quartz | ¥400–600 | ¥600–900 | ¥900–1500 |
| Solid Surface | ¥400–600 | ¥600–900 | ¥900–1200 |
| Stainless Steel | ¥500–700 | ¥700–900 | ¥900–1200 |
| Granite | ¥600–900 | ¥900–1500 | ¥1500–2000+ |
| Sintered Stone | ¥800–1200 | ¥1200–1800 | ¥1800–2500+ |
| Marble | ¥800–1200 | ¥1200–2000 | ¥2000–3000+ |

## 10. Selection Guide by Room and Usage

### Kitchen Countertop

| Usage Pattern | Recommended Material | Thickness | Edge Profile |
| --- | --- | --- | --- |
| Heavy cooking, Chinese cuisine | Quartz or Sintered Stone | 20mm | Eased or beveled |
| Baking-focused (pastry) | Marble or Quartz | 20–30mm | Bullnose or eased |
| Modern / minimalist | Stainless Steel or Sintered Stone | 1.5mm / 12mm | Square edge |
| Budget / rental | Laminate | 28mm total | Post-formed |
| Seamless look with integrated sink | Solid Surface | 12mm | Integrated |
| Traditional / luxury | Granite | 30mm | Bullnose or ogee |

### Bathroom Vanity

| Priority | Recommended Material | Why |
| --- | --- | --- |
| Hygiene first | Solid Surface (seamless with basin) | No joints for bacteria |
| Luxury look | Marble | Elegant veining |
| Durability | Quartz | Stain-resistant, low maintenance |
| Budget | Laminate or Ceramic tile | Cost-effective |

### Outdoor Kitchen

| Material | Suitability | Notes |
| --- | --- | --- |
| Granite | Excellent | UV stable, weather resistant |
| Sintered Stone | Excellent | Best overall for outdoors |
| Stainless Steel | Good | 316 grade for coastal areas |
| Quartz | Poor | UV may cause yellowing |
| Marble | Poor | Weathering and staining |
| Laminate | Not suitable | Water damage |

## 11. Countertop Installation Checklist

- Verify cabinet top is level (±2mm over 2m) before templating

- Measure and template AFTER cabinets are installed (not before)

- Specify cutout locations for sink, cooktop, faucet in advance

- Undermount sink requires reinforced substrate and clips

- Allow 2–3mm expansion gap at wall; cover with backsplash or silicone

- Seams should be placed away from high-use areas; request color-matched adhesive

- Overhang beyond 300mm requires brackets or corbels (for stone)

- For cooktops, verify clearance between countertop and appliances below

- Inspect slab in person before cutting (natural stone varies)

- Request installation photos showing seam quality and edge finish

- Water test around sink cutout after installation (check for leaks)

- Retain manufacturer warranty card and product certificate

## 12. Edge Profile Options

| Profile | Description | Best For | Cost Impact |
| --- | --- | --- | --- |
| Square / Eased | Clean 90° with slight rounding | Modern, minimalist | Base |
| Beveled | Angled cut (usually 45°) | Transitional | +10–15% |
| Bullnose | Fully rounded edge | Traditional, family kitchens | +15–25% |
| Half Bullnose | Rounded top, square bottom | Budget traditional | +10% |
| Ogee | Decorative S-curve | Luxury, ornate styles | +30–50% |
| Waterfall | Vertical continuation to floor | Kitchen islands, modern | +50–100% (material + labor) |
| Mitered | 45° joint creating thick appearance | Premium, sintered stone | +20–30% |

# 窗帘选购指南

## 窗帘类型

| 类型 | 特点 | 适用场景 |
| --- | --- | --- |
| 布艺窗帘 | 遮光好、温馨 | 卧室 |
| 纱帘 | 透光不透人 | 客厅 |
| 百叶窗 | 调光灵活 | 书房、卫生间 |
| 卷帘 | 简洁 | 办公室、厨房 |
| 罗马帘 | 美观 | 客厅、卧室 |

## 遮光度选择

| 空间 | 遮光度 |
| --- | --- |
| 客厅 | 30-50% |
| 卧室 | 70-90% |
| 书房 | 50-70% |
| 儿童房 | 50-70% |

## 材质选择

| 材质 | 特点 | 价格 |
| --- | --- | --- |
| 棉麻 | 自然、透气 | 中 |
| 绒布 | 保暖、高档 | 高 |
| 涤纶 | 耐用、便宜 | 低 |
| 纱 | 透光、轻盈 | 中 |

## 颜色搭配

- 与墙面同色系：安全百搭

- 与家具呼应：整体协调

- 对比色：增加层次

## 安装方式

| 方式 | 特点 |
| --- | --- |
| 窗帘盒 | 美观、隐藏轨道 |
| 罗马杆 | 简洁、易安装 |
| 轨道 | 实用、经济 |

## 尺寸计算

窗帘宽度 = 窗户宽度 × 1.5-2（褶皱倍数）
窗帘高度 = 轨道到地面距离

## 价格参考

| 档次 | 价格（元/米） |
| --- | --- |
| 经济 | 30-80 |
| 中档 | 80-200 |
| 高档 | 200-500 |

# 全屋定制详解

## 定制类型

| 类型 | 包含内容 | 适用场景 |
| --- | --- | --- |
| 橱柜定制 | 厨房地柜、吊柜 | 厨房 |
| 衣柜定制 | 卧室衣柜 | 卧室 |
| 书柜定制 | 书房书柜 | 书房 |
| 鞋柜定制 | 玄关鞋柜 | 玄关 |
| 全屋定制 | 所有柜体 | 全屋 |

## 板材选择

| 板材 | 特点 | 环保性 | 价格 |
| --- | --- | --- | --- |
| 颗粒板 | 稳定性好 | E0/ENF | 中 |
| 多层板 | 防潮好 | E0/ENF | 中高 |
| 生态板 | 免漆环保 | E0/ENF | 高 |
| 密度板 | 可造型 | E1/E0 | 低 |

## 五金选择

| 配件 | 推荐品牌 | 说明 |
| --- | --- | --- |
| 铰链 | 百隆、海蒂诗 | 带缓冲 |
| 滑轨 | 百隆、海蒂诗 | 三节导轨 |
| 拉手 | 根据风格 | 隐形拉手流行 |

## 计价方式

### 投影面积计价

总价 = 投影面积 × 单价

### 展开面积计价

总价 = 各部件展开面积 × 单价

## 选购流程

- 量尺

- 设计

- 选材料

- 报价

- 生产（15-30天）

- 安装（1-3天）

- 验收

# 全屋定制选购指南

## 定制类型

| 类型 | 包含内容 | 价格区间（元/㎡投影面积） |
| --- | --- | --- |
| 橱柜定制 | 厨房地柜、吊柜 | 800-2000 |
| 衣柜定制 | 卧室衣柜 | 600-1500 |
| 全屋定制 | 橱柜+衣柜+鞋柜+电视柜等 | 2万-8万 |

## 板材选择

| 板材 | 特点 | 环保性 | 价格 |
| --- | --- | --- | --- |
| 颗粒板 | 稳定性好、性价比高 | E0/ENF | 中 |
| 多层板 | 防潮性好 | E0/ENF | 中高 |
| 生态板 | 免漆、环保 | E0/ENF | 高 |
| 密度板 | 可造型 | E1/E0 | 低 |

## 五金配件

五金是定制家具的灵魂，直接影响使用寿命：

| 配件 | 推荐品牌 | 备注 |
| --- | --- | --- |
| 铰链 | 百隆、海蒂诗、DTC | 带缓冲 |
| 滑轨 | 百隆、海蒂诗 | 三节导轨 |
| 拉手 | 根据风格选择 | 隐形拉手流行 |

## 计价方式

### 投影面积计价

总价 = 投影面积 × 单价

- 简单透明

- 但内部格局变化不影响价格

### 展开面积计价

总价 = 各部件展开面积 × 各部件单价

- 精确但复杂

- 容易有隐性增项

## 选购流程

- 量尺：设计师上门量尺

- 设计：出设计图和效果图

- 选材料：选板材、颜色、五金

- 报价：确认报价和方案

- 生产：工厂生产（15-30 天）

- 安装：现场安装（1-3 天）

- 验收：检查质量和五金

## 避坑要点

- 确认板材环保等级（要求检测报告）

- 明确五金品牌和型号

- 确认是否包含安装和运输

- 约定生产周期和延期赔偿

- 验收时检查封边、孔位、五金

# 室内门选购指南

## 门的类型

| 类型 | 价格（元/扇） | 优点 | 缺点 | 适用场景 |
| --- | --- | --- | --- | --- |
| 实木门 | 2000-8000 | 质感好、隔音好 | 价格高、易变形 | 卧室、书房 |
| 实木复合门 | 1000-3000 | 性价比高、稳定性好 | 隔音一般 | 卧室、书房 |
| 模压门 | 500-1200 | 价格便宜 | 质感差、隔音差 | 出租房 |
| 玻璃门 | 800-2500 | 采光好、现代感 | 隐私性差 | 厨房、卫生间 |
| 铝合金门 | 600-1500 | 防潮、耐用 | 质感一般 | 卫生间、阳台 |

## 选购要点

### 材质

- 实木门看木材种类（橡木、胡桃木、樱桃木）

- 实木复合门看芯材和贴面

- 检查封边是否严密

### 隔音性能

- 门芯填充：桥洞力学板 > 蜂窝纸

- 门缝密封：三元乙丙密封条 > 普通密封条

- 门厚度：45mm > 40mm > 35mm

### 五金配件

- 合页：不锈钢合页，每扇门至少 3 个

- 门锁：静音锁体

- 门吸：地吸或墙吸

## 门的尺寸

| 位置 | 标准尺寸（宽×高） |
| --- | --- |
| 卧室门 | 800×2100mm |
| 卫生间门 | 700×2100mm |
| 厨房门 | 750×2100mm（或推拉门） |
| 入户门 | 960×2050mm |

## 安装验收

- 门框垂直度≤2mm/2m

- 门扇与地面间隙 5-8mm

- 开合顺畅无异响

- 密封条严密无漏光

# 装修环保材料详解

## 板材环保等级

| 等级 | 甲醛释放量 | 说明 |
| --- | --- | --- |
| ENF | ≤0.025mg/m³ | 最高标准 |
| E0 | ≤0.050mg/m³ | 推荐标准 |
| E1 | ≤0.124mg/m³ | 国标底线 |

## 涂料环保指标

| 指标 | 国标限值 | 优质产品 |
| --- | --- | --- |
| VOC | ≤200g/L | ≤50g/L |
| 甲醛 | ≤100mg/kg | ≤50mg/kg |
| 苯 | ≤300mg/kg | ≤100mg/kg |

## 环保材料选择

### 板材

- 实木 > 多层 > 颗粒 > 密度板

### 涂料

- 水性漆 > 油性漆

### 胶水

- 环保胶 > 普通胶

## 环保检测

- 装修后封闭12小时检测

- 甲醛≤0.08mg/m³建议值

- 请专业机构检测

# 装修环保材料指南

## 环保标准

| 标准 | 甲醛释放量 | 说明 |
| --- | --- | --- |
| ENF级 | ≤0.025mg/m³ | 最高标准 |
| E0级 | ≤0.050mg/m³ | 推荐标准 |
| E1级 | ≤0.124mg/m³ | 国标底线 |

## 环保材料选择

### 板材

- 实木板 > 多层板 > 颗粒板

- 选择ENF级

- 避免密度板

### 涂料

- 水性漆 > 油性漆

- VOC含量≤50g/L

- 十环认证

### 胶水

- 环保胶

- 减少使用量

- 物理连接替代

## 环保施工

- 减少胶水使用

- 做好通风

- 材料分类存放

## 环保检测

| 指标 | 标准 | 建议值 |
| --- | --- | --- |
| 甲醛 | ≤0.10mg/m³ | ≤0.08mg/m³ |
| 苯 | ≤0.11mg/m³ | ≤0.08mg/m³ |
| TVOC | ≤0.60mg/m³ | ≤0.50mg/m³ |

# 地板种类详解

## 按材质分类

| 类型 | 特点 | 价格 | 适用场景 |
| --- | --- | --- | --- |
| 实木地板 | 天然环保 | 200-800/㎡ | 卧室、书房 |
| 实木复合 | 稳定性好 | 150-400/㎡ | 客厅、卧室 |
| 强化地板 | 耐磨便宜 | 80-200/㎡ | 客厅、书房 |
| SPC石塑 | 防水环保 | 80-180/㎡ | 厨卫、阳台 |

## 按安装方式分类

| 方式 | 特点 |
| --- | --- |
| 锁扣式 | 安装简便 |
| 平扣式 | 需要胶水 |
| 龙骨式 | 实木专用 |

## 选购要点

- 环保等级（ENF > E0 > E1）

- 耐磨转数（家用≥6000转）

- 含水率（8-13%）

- 表面质量（无划痕、无变形）

# 地板选购指南

## 地板类型对比

| 类型 | 价格（元/㎡） | 优点 | 缺点 | 适用场景 |
| --- | --- | --- | --- | --- |
| 实木地板 | 200-800 | 天然环保、脚感好 | 价格高、需保养 | 卧室、书房 |
| 实木复合 | 150-400 | 稳定性好、性价比高 | 胶水粘合 | 客厅、卧室 |
| 强化地板 | 80-200 | 耐磨、便宜 | 脚感硬、环保性一般 | 客厅、书房 |
| SPC石塑 | 80-180 | 防水、环保 | 脚感一般 | 厨卫、阳台 |

## 实木地板选购

### 材种选择

- 橡木：纹理清晰、硬度高、价格中高

- 柚木：稳定性好、防腐、价格高

- 胡桃木：色泽深沉、高档、价格高

- 桦木：纹理细腻、价格中等

- 番龙眼：性价比高、入门级

### 等级区分

- A级：无明显缺陷，纹理清晰

- B级：有少量天然缺陷

- C级：缺陷较多，价格便宜

## 实木复合地板选购

### 层数选择

- 三层：表层厚、脚感好、价格高

- 多层：稳定性好、价格适中

- 建议选表层厚度≥2mm的

### 胶水环保性

- 选择 E0 级或 ENF 级环保标准

- 看甲醛释放量检测报告

## 强化地板选购

### 耐磨转数

- 家用≥6000 转

- 商用≥9000 转

### 基材

- 选择高密度纤维板（HDF）

- 看截面密度是否均匀

## 安装注意事项

- 安装前地面必须找平

- 铺设防潮垫，接缝处重叠

- 地板与墙面之间留伸缩缝

- 实木地板需要打龙骨

- 安装后 24 小时内不要放重物

## 验收要点

| 检查项目 | 标准要求 |
| --- | --- |
| 平整度 | ≤3mm/2m |
| 接缝高低差 | ≤0.5mm |
| 踢脚线与墙面 | 紧密无缝隙 |
| 踩踏响声 | 无异响 |
| 表面 | 无划痕、无磕碰 |

# 五金选购指南

## 五金包含内容

- 铰链

- 滑轨

- 拉手

- 门锁

- 合页

- 地吸/门吸

- 角阀

- 软管

- 地漏

- 毛巾架

- 置物架

## 铰链选择

| 品牌 | 档次 | 价格（元/个） | 特点 |
| --- | --- | --- | --- |
| 百隆 Blum | 高端 | 15-30 | 带缓冲 |
| 海蒂诗 Hettich | 高端 | 12-25 | 带缓冲 |
| DTC | 中端 | 5-15 | 性价比高 |
| 国产杂牌 | 低端 | 1-5 | 易坏 |

## 滑轨选择

| 类型 | 特点 | 价格 |
| --- | --- | --- |
| 二节轨 | 基础款 | 10-20 |
| 三节轨 | 拉出更长 | 15-30 |
| 隐藏轨 | 美观 | 20-40 |
| 骑马抽 | 高端 | 50-100 |

## 门锁选择

| 类型 | 价格 | 特点 |
| --- | --- | --- |
| 机械锁 | 50-200 | 基础款 |
| 智能锁 | 1000-5000 | 指纹/密码开锁 |
| 静音锁 | 100-300 | 锁体静音 |

## 地漏选择

| 类型 | 特点 | 适用场景 |
| --- | --- | --- |
| U型地漏 | 防臭好 | 淋浴区 |
| T型地漏 | 排水快 | 干区 |
| 硅胶地漏 | 便宜 | 临时用 |

## 选购建议

- 五金是家具的灵魂，不能省

- 选择知名品牌

- 带缓冲的铰链体验更好

- 五金提前确认数量

# 材料鉴别

## 瓷砖鉴别

- 看平整度：两块砖面对面贴合，缝隙应均匀

- 听声音：敲击声音清脆说明密度高

- 看吸水率：滴水测试，吸水慢说明质量好

## 电线鉴别

- 看 3C 认证标识

- 看铜芯颜色：应为紫红色，发白发暗为次品

- 量线径：用卡尺测量，偏差应在国标范围内

## 水管鉴别

- 看管壁厚度：符合国标

- 闻气味：优质 PPR 管无异味

- 看标识：品牌、规格、生产日期清晰

## 涂料鉴别

- 开盖观察：优质涂料表面无硬皮、无分层

- 闻气味：环保涂料气味淡

- 看检测报告：VOC、甲醛含量达标

# 保温隔热材料指南 (Insulation Materials Guide)

## 1. Why Insulation Matters in Renovation

Proper insulation reduces energy costs by 20–40%, improves thermal comfort, reduces condensation and mold risk, and provides acoustic benefits. In renovation projects, insulation upgrades are most cost-effective when walls, windows, or roofs are already being opened up.

### Key Metrics

| Term | Symbol | Definition | Unit |
| --- | --- | --- | --- |
| Thermal Conductivity | λ (lambda) | Heat flow through 1m thickness per 1°C difference | W/(m·K) — lower is better |
| Thermal Resistance | R-value | Thickness / conductivity; resistance to heat flow | m²·K/W — higher is better |
| U-Value | U | Overall heat transfer coefficient of an assembly | W/(m²·K) — lower is better |
| R-Value (US) | R-US | Imperial resistance | ft²·°F·h/BTU |

### Conversion

- R-value (metric) = thickness (m) / λ

- R-US ≈ R-metric × 5.678

## 2. Insulation Material Types

### Material Comparison Table

| Material | Chinese Name | λ (W/m·K) | Form | R-value per 50mm | Fire Rating | Cost (per m², 50mm) | Best Use |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Expanded Polystyrene (EPS) | 膨胀聚苯板 (EPS) | 0.032–0.038 | Rigid board | ~1.3–1.6 | B1 (flame-retardant) | Low | Exterior wall insulation |
| Extruded Polystyrene (XPS) | 挤塑聚苯板 (XPS) | 0.028–0.034 | Rigid board | ~1.5–1.8 | B1/B2 | Low–Mid | Floor, roof, below-grade |
| Rock Wool / Mineral Wool | 岩棉板 | 0.034–0.040 | Board or batt | ~1.25–1.47 | A (non-combustible) | Mid | Fire-rated walls, facades |
| Glass Wool | 玻璃棉 | 0.032–0.044 | Roll / batt | ~1.1–1.56 | A (non-combustible) | Low–Mid | Ceiling, stud wall cavities |
| Polyurethane Foam (PUR/PIR) | 聚氨酯板 | 0.022–0.028 | Rigid board / spray | ~1.8–2.3 | B1/B2 | High | Roof, thin-profile walls |
| Aerogel Blanket | 气凝胶毡 | 0.014–0.020 | Flexible blanket | ~2.5–3.6 | A | Very High | Space-constrained retrofits |
| Phenolic Foam | 酚醛板 | 0.018–0.025 | Rigid board | ~2.0–2.8 | B1 | High | Fire-sensitive applications |
| Reflective Foil (Radiant Barrier) | 铝箔反射隔热膜 | N/A (reflective) | Sheet / roll | ~0.3–0.8 (effective) | Varies | Low | Attic / roof radiant barrier |

## 3. Wall Insulation (墙体保温)

### Exterior Wall Insulation (外保温)

The most effective approach — wraps the entire building envelope.

#### Common Systems

| System Type | Description | Thickness | Typical R-value | Suitable For |
| --- | --- | --- | --- | --- |
| EIFS (External Insulation Finish System) | Insulation board + adhesive + mesh + finish coat | 50–120mm | 1.5–4.0 | New construction, major renovation |
| Ventilated Facade (幕墙) | Insulation + air gap + cladding panel | 60–150mm | 1.7–4.5 | Commercial, high-end residential |
| Insulating Render (保温砂浆) | Lightweight insulating plaster | 20–40mm | 0.5–1.0 | Heritage buildings, thin-profile retrofit |

#### EPS Board Installation Steps

- Clean and level wall surface

- Apply adhesive in dot-and-perimeter pattern (minimum 40% coverage)

- Press boards firmly, staggering joints in brick pattern

- Wait 24 hours for adhesive set

- Install mechanical anchors (6–8 per m², depending on height)

- Apply base coat with embedded fiberglass mesh

- Apply finish coat (textured render or paint)

#### EPS Board Installation Checklist

- Surface must be dry, clean, and structurally sound

- Boards must be cut tightly around openings (no gaps > 2mm)

- Stagger vertical joints — never align joints at corners

- Anchor spacing: 6 per m² below 20m height, 8+ above

- Mesh overlap at joints: minimum 100mm

- Temperature during installation: 5–35°C

- Do NOT install in rain or on wet substrate

### Interior Wall Insulation (内保温)

Used when exterior insulation is not possible (heritage buildings, apartments, space constraints).

| Material | Recommended Thickness | Notes |
| --- | --- | --- |
| XPS board | 20–40mm | Thin profile, good performance |
| Aerogel blanket | 10–20mm | Premium, space-saving |
| Phenolic board | 20–30mm | Fire-safe, thin |
| Insulating plaster | 15–30mm | DIY-friendly, lower performance |

Warning: Interior insulation creates a cold bridge at floor/ceiling junctions and can cause interstitial condensation. Always install a vapor barrier on the warm side (facing the room).

## 4. Window Insulation (窗户隔热)

### Window U-Values by Configuration

| Window Type | Glass | Frame | U-Value (W/m²·K) | SHGC |
| --- | --- | --- | --- | --- |
| Single glazed | Clear single pane | Aluminum (no thermal break) | 5.7–6.5 | 0.85 |
| Double glazed | 5+12A+5 clear | Aluminum thermal break | 2.7–3.2 | 0.70 |
| Double glazed | Low-E + argon | Aluminum thermal break | 1.6–2.0 | 0.40 |
| Triple glazed | Low-E + argon x2 | PVC / wood | 0.8–1.2 | 0.35 |
| Double glazed | Low-E + warm edge spacer | Wood-clad aluminum | 1.1–1.4 | 0.38 |

### Window Insulation Upgrade Checklist

- Replace single-glazed windows minimum with double Low-E

- Verify thermal break on all aluminum frames

- Check weatherstripping condition; replace worn seals

- Install window insulation film in winter (temporary)

- Seal frame-to-wall gap with low-expansion PU foam

- Apply silicone sealant on exterior perimeter

- Consider insulated shutters or blinds for summer heat rejection

- Verify spacer type: warm edge (thermoplastic) outperforms aluminum spacer

### Glass Types Explained

| Glass Type | Description | Benefit |
| --- | --- | --- |
| Low-E (低辐射玻璃) | Microscopically thin metallic coating reflects IR | Reduces heat transfer 30–50% |
| Tinted / Reflective | Absorbs or reflects solar radiation | Reduces solar heat gain |
| Laminated | Two panes with PVB interlayer | Safety + acoustic + UV protection |
| Tempered | Heat-strengthened | Safety (shatters into small pieces) |
| Electrochromic / Smart Glass | Electrically switchable tint | Dynamic solar control, expensive |

## 5. Roof Insulation (屋顶保温)

### Roof Insulation Methods

| Method | Description | Material | Thickness | R-value Range |
| --- | --- | --- | --- | --- |
| Above-deck (inverted) | Insulation above structural deck, under waterproofing | XPS board | 60–120mm | 1.8–3.6 |
| Below-deck (warm roof) | Insulation below deck, between rafters | Mineral wool, PIR board | 100–200mm | 2.5–7.0 |
| Spray foam | Closed-cell PU sprayed on underside | PU foam | 50–100mm | 1.8–3.6 |
| Loose fill (attic) | Blown cellulose or glass wool in attic space | Cellulose, glass wool | 150–300mm | 3.5–8.0 |
| Reflective foil | Radiant barrier under roof covering | Multi-layer foil | N/A | 0.3–0.8 effective |

### Recommended Roof R-Values by Climate

| Climate Zone | Minimum Roof R-value (metric) | Equivalent Thickness (Mineral Wool) |
| --- | --- | --- |
| Hot-humid (South China) | 2.0 | ~70mm |
| Mixed / temperate (East China) | 3.0 | ~100mm |
| Cold (North China) | 4.0 | ~130mm |
| Severe cold (Northeast) | 5.0+ | ~170mm+ |

### Installation Checklist — Below-Deck Insulation

- Ensure roof waterproofing is intact before insulating

- Provide ventilation gap (50mm minimum) between insulation and roof deck

- Install vapor barrier on warm side (ceiling side)

- Do NOT compress batt insulation — it loses R-value

- Seal all penetrations (wires, pipes, light fixtures) through the vapor barrier

- Use fire-rated insulation (Class A) near chimneys or heat sources

- Verify insulation does not block soffit/eave ventilation channels

## 6. Floor Heating Insulation (地暖保温层)

### Floor Heating System Layers (bottom to top)

| Layer | Material | Thickness | Purpose |
| --- | --- | --- | --- |
| 1. Structural slab | Concrete | 100mm+ | Base structure |
| 2. Waterproofing | SBS membrane or coating | 2–3mm | Moisture barrier (ground floor) |
| 3. Insulation board | XPS or EPS | 20–30mm | Prevent downward heat loss |
| 4. Reflective film | Aluminum foil | 0.2mm | Reflect heat upward |
| 5. Wire mesh | Steel mesh | 2–3mm | Support and protect pipe |
| 6. Heating pipe | PEX-a or PERT | 16–20mm | Heat distribution |
| 7. Backfill / screed | Concrete or anhydrite | 40–50mm above pipe | Thermal mass and surface leveling |
| 8. Floor finish | Tile, wood, etc. | Varies | Final surface |

### Insulation Board Requirements

| Property | Minimum Requirement |
| --- | --- |
| Compressive strength | ≥ 150 kPa (for residential) / ≥ 250 kPa (commercial) |
| Thermal conductivity | ≤ 0.035 W/(m·K) |
| Water absorption | ≤ 1.5% by volume |
| Fire rating | B1 minimum |
| Thickness | 20mm minimum (ground floor: 30mm recommended) |

### Floor Heating Insulation Checklist

- Ground floor: install waterproofing layer before insulation

- Upper floors: 20mm XPS minimum; 30mm for better efficiency

- Perimeter: install edge insulation strip (10–15mm) around all walls

- Reflective film: seams overlapped and taped

- Pipe spacing: 150–200mm (closer near exterior walls/windows)

- Pressure test heating pipes before screed pour

- Screed must cure 21 days before turning on heating

- Gradual heat-up: increase temperature 5°C per day during first commissioning

## 7. Fire Safety Considerations

### Insulation Material Fire Ratings

| Rating | Description | Approved Materials |
| --- | --- | --- |
| A (Non-combustible) | Will not burn | Rock wool, glass wool, aerogel |
| B1 (Flame-retardant) | Difficult to ignite, self-extinguishing | EPS B1, XPS B1, PIR |
| B2 (Combustible) | Ignites but slow spread | EPS B2, PU foam |
| B3 (Flammable) | No fire resistance | Unmodified polystyrene — banned in building |

### Fire Safety Rules

- Buildings above 27m height: exterior insulation must be Class A

- Buildings 24–27m: minimum Class B1 with fire barriers every 2 floors

- Fire barriers: horizontal mineral wool bands at each floor level (300mm minimum height)

- All insulation must be fully covered with fire-rated render or cladding

- Never leave exposed foam insulation on any building interior

## 8. Condensation and Vapor Control

### The Dew Point Rule

When warm, moist indoor air meets a cold surface, condensation occurs. Insulation changes the temperature profile within the wall, and the dew point may shift.

| Scenario | Risk | Solution |
| --- | --- | --- |
| Interior insulation without vapor barrier | High — condensation within wall | Install vapor barrier on warm side |
| Exterior insulation | Low — structure stays warm | No vapor barrier needed typically |
| Roof insulation without ventilation | High — condensation on underside of deck | Provide ventilation gap or use vapor-open insulation |
| Ground floor without waterproofing | Moderate — rising damp through insulation | SBS membrane under insulation |

### Vapor Barrier Installation Checklist

- Use polyethylene sheet (0.2mm minimum) or vapor-retarding membrane

- Overlap seams by 200mm; seal with vapor barrier tape

- Seal around all penetrations (outlets, pipes)

- Continuous — no gaps or tears

- On warm side of insulation (room side for interior insulation)

- Verify with blower door test if possible

## 9. Selection Guide by Renovation Scenario

| Scenario | Recommended Insulation | Thickness | Estimated R-value |
| --- | --- | --- | --- |
| Exterior wall (new build) | EPS board B1 | 80mm | 2.4 |
| Exterior wall (retrofit) | EPS board B1 or mineral wool | 60mm | 1.8 |
| Interior wall (space-constrained) | Aerogel blanket or phenolic board | 20mm | 0.8–1.0 |
| Flat roof | XPS inverted roof system | 100mm | 3.0 |
| Pitched roof (between rafters) | Mineral wool batts | 150mm | 4.0 |
| Attic floor | Blown cellulose | 200mm | 5.0 |
| Floor heating (upper floor) | XPS board | 20mm | 0.6 |
| Floor heating (ground floor) | XPS board + waterproofing | 30mm | 0.9 |
| Window upgrade | Double Low-E + thermal break frame | N/A | U-value 1.6–2.0 |
| Pipe insulation (hot water) | Rubber foam tube | 20mm wall | Prevents heat loss and condensation |
| Hot water tank | PU foam or fiberglass wrap | 50mm | Reduces standby losses 50%+ |

## 10. Brand and Product Recommendations

| Brand | Product Range | Notes |
| --- | --- | --- |
| Knauf (可耐福) | Glass wool, mineral wool, EIFS | Global leader, full system |
| Rockwool (洛科威) | Mineral wool boards and batts | Fire-safe, acoustic benefits |
| Owens Corning | Fiberglass, foam board | Wide availability |
| BASF | PIR/PUR boards, spray foam | Chemical manufacturer, high performance |
| Saint-Gobain (Isover) | Glass wool, mineral wool | European quality |
| Local XPS manufacturers | Various | Verify compressive strength and fire rating on test report |

### Purchasing Checklist

- Request material test report (导热系数, 燃烧等级, 抗压强度)

- Verify fire rating certificate from accredited lab

- Check manufacturing date — aged EPS/XPS loses some performance

- Buy from authorized distributor to avoid counterfeit products

- For exterior systems, use complete system from one manufacturer (board + adhesive + mesh + render)

- Retain all product documentation for building inspection records

# 灯具选购指南

## 灯具类型

| 类型 | 用途 | 安装位置 |
| --- | --- | --- |
| 吸顶灯 | 基础照明 | 客厅、卧室 |
| 吊灯 | 装饰+照明 | 餐厅、客厅 |
| 筒灯 | 局部照明 | 吊顶内 |
| 射灯 | 重点照明 | 墙面、展品 |
| 灯带 | 氛围照明 | 吊顶、柜内 |
| 壁灯 | 辅助照明 | 床头、走廊 |
| 落地灯 | 移动照明 | 沙发旁 |
| 台灯 | 桌面照明 | 书桌、床头 |

## 光源选择

### 色温

| 色温 | 光色 | 适用场景 |
| --- | --- | --- |
| 2700-3000K | 暖白 | 卧室、餐厅 |
| 4000K | 自然白 | 客厅、书房 |
| 5000-6500K | 冷白 | 厨房、卫生间 |

### 显色指数

- ≥90：博物馆级，还原真实色彩

- ≥80：家用推荐

- ≥70：最低标准

### 功率参考

| 空间 | 功率（W/㎡） |
| --- | --- |
| 客厅 | 3-5 |
| 卧室 | 2-3 |
| 书房 | 5-7 |
| 厨房 | 3-5 |

## 智能灯具

- WiFi/蓝牙连接

- 可调色温亮度

- 语音控制

- 场景模式

## 选购建议

- 客厅：吸顶灯+筒灯+灯带

- 卧室：吸顶灯+床头灯

- 餐厅：吊灯

- 厨房：集成吊顶灯+吊柜灯带

- 卫生间：集成吊顶灯+镜前灯

## 价格参考

| 档次 | 全屋灯具预算 |
| --- | --- |
| 经济 | 2000-5000 |
| 中档 | 5000-15000 |
| 高档 | 15000-50000 |

# 装修主材清单详解

## 瓷砖

| 空间 | 规格 | 数量 |
| --- | --- | --- |
| 客厅 | 800×800 | 按面积计算 |
| 厨卫墙面 | 300×600 | 按面积计算 |
| 厨卫地面 | 300×300 | 按面积计算 |

## 地板

| 空间 | 类型 | 数量 |
| --- | --- | --- |
| 卧室 | 实木复合 | 按面积计算 |
| 客厅 | 瓷砖或地板 | 按面积计算 |

## 门

| 位置 | 类型 | 数量 |
| --- | --- | --- |
| 入户 | 防盗门 | 1扇 |
| 卧室 | 室内门 | N扇 |
| 卫生间 | 防水门 | N扇 |

## 橱柜

- 厨房地柜：按长度计算

- 厨房吊柜：按长度计算

- 台面：按长度计算

## 卫浴

- 马桶：1-2个

- 花洒：1-2套

- 浴室柜：1-2个

## 其他

- 涂料：按面积计算

- 开关插座：按数量计算

- 灯具：按数量计算

# 主材清单

装修主材是装修费用的大头，以下是完整的主材清单：

## 瓷砖类

- 地砖

- 墙砖

- 厨卫墙砖

- 阳台砖

## 地板类

- 实木地板

- 复合地板

- 强化地板

- 踢脚线

## 门类

- 入户门

- 室内门（卧室、书房）

- 卫生间门

- 厨房推拉门

## 橱柜

- 整体橱柜

- 台面（石英石/岩板）

## 卫浴

- 马桶/智能马桶

- 花洒

- 浴室柜

- 淋浴房

## 吊顶

- 厨卫集成吊顶

- 客厅卧室吊顶材料

## 其他

- 石材窗台

- 开关面板

- 灯具

# 涂料选购与施工指南

## 涂料类型

| 类型 | 特点 | 适用场景 |
| --- | --- | --- |
| 乳胶漆 | 环保、易施工 | 客厅、卧室 |
| 水性漆 | 更环保、无味 | 儿童房 |
| 艺术涂料 | 质感丰富 | 背景墙 |
| 硅藻泥 | 调湿、净化空气 | 卧室、客厅 |

## 乳胶漆选购

### 关键指标

- VOC 含量：≤50g/L（国标），越低越环保

- 甲醛含量：≤100mg/kg

- 遮盖力：遮盖力越强越省漆

- 耐擦洗性：≥5000 次为优

### 品牌推荐

| 档次 | 品牌 | 价格（元/桶 5L） |
| --- | --- | --- |
| 高端 | 芬琳、都芳 | 800-1500 |
| 中高端 | 多乐士、立邦高端 | 400-800 |
| 中端 | 三棵树、嘉宝莉 | 200-400 |
| 经济 | 立邦、多乐士基础款 | 100-200 |

### 颜色选择

- 采光好：可以选择深色或冷色调

- 采光差：选择浅色暖色调

- 小空间：浅色系显大

- 大空间：可以局部用深色增加层次

## 施工工艺

### 墙面处理

- 清理墙面

- 修补裂缝和孔洞

- 批刮腻子 2-3 遍

- 打磨平整

- 刷底漆 1 遍

- 刷面漆 2 遍

### 关键要点

- 每遍间隔 4-6 小时

- 施工温度 5-35°C

- 施工湿度≤85%

- 涂刷方向一致

## 用量计算

用漆量 = 涂刷面积 × 2（遍）÷ 每桶覆盖面积

一般 5L 乳胶漆可涂刷 35-40㎡（一遍）

## 验收要点

- 表面平整光滑

- 无色差、无透底

- 无流坠、无刷痕

- 阴阳角线条顺直

# 水管电线管材详解 (Pipe & Wire Materials Guide)

## 1. Water Pipe Materials: PPR vs PEX vs Copper

### Overview Comparison Table

| Feature | PPR Pipe | PEX Pipe | Copper Pipe |
| --- | --- | --- | --- |
| Full Name | Polypropylene Random Copolymer | Cross-linked Polyethylene | Copper Alloy |
| Service Life | 50+ years | 50+ years | 70+ years |
| Max Temperature | 95°C | 93°C | 250°C+ |
| Connection Method | Hot melt (thermofusion) | Compression / crimp fittings | Soldering / brazing / press-fit |
| Corrosion Resistance | Excellent | Excellent | Good (may develop patina) |
| Bacteria Growth | Low | Low | Very low (copper is antimicrobial) |
| UV Resistance | Poor (not for outdoor) | Moderate | Excellent |
| Cost | Low (most economical) | Moderate | High (3–5x PPR) |
| Installation Difficulty | Easy (requires hot melt tool) | Moderate (requires special fittings) | Difficult (requires soldering skill) |
| Flexibility | Rigid (uses elbow fittings) | Flexible (can bend) | Rigid (uses elbow fittings) |
| Typical Applications | Residential water supply | Radiant floor heating, repipes | High-end residential, commercial |

### PPR Pipe (无规共聚聚丙烯管)

#### Classification

- Cold Water PPR (S5/S4 series): Wall thickness 2.0–3.4mm, rated for cold water only

- Hot Water PPR (S3.2/S2.5 series): Wall thickness 2.8–4.6mm, rated for hot water up to 95°C

- Color Coding: White, green, or gray — color does NOT indicate quality; wall thickness and series number do

#### Key Specifications

| Nominal Diameter (DN) | Outer Diameter (mm) | Wall Thickness (Hot Water S2.5) | Typical Use |
| --- | --- | --- | --- |
| DN15 | 20mm | 3.4mm | Branch lines (faucets, toilets) |
| DN20 | 25mm | 4.2mm | Branch lines (showers) |
| DN25 | 32mm | 4.4mm | Main distribution |
| DN32 | 40mm | 5.5mm | Main inlet line |
| DN50 | 63mm | 7.1mm | Building main supply |

#### Installation Checklist

- Verify pipe series matches application (hot water pipe for hot water lines)

- Cut pipe perpendicular with dedicated pipe cutter — do NOT use a saw

- Clean pipe ends and fittings before hot melt

- Heat to 260°C; over-heating degrades material, under-heating causes weak joints

- Hold joint steady during cooling (minimum 30 seconds for DN20)

- Pressure test at 1.5x working pressure for 1+ hours before closing walls

- Mark pipe run locations on wall photos before plastering

### PEX Pipe (交联聚乙烯管)

#### Types

| Type | Cross-linking Method | Key Characteristics |
| --- | --- | --- |
| PEX-a | Peroxide (Engel) method | Most flexible, highest cross-linking (~75%), best memory/shape recovery |
| PEX-b | Silane method | Stiffer, moderate cost, most common in China |
| PEX-c | Electron beam (radiation) | Least flexible, budget option |

#### Best Use Cases

- Radiant floor heating loops (PEX-a preferred for flexibility)

- Repiping inside existing walls (can snake through cavities)

- Snow melting systems

- NOT recommended for exposed runs (UV degradation)

### Copper Pipe (铜管)

#### Grades

| Grade | Wall Thickness | Common Use |
| --- | --- | --- |
| Type M | Thinnest | Dry plumbing, residential water |
| Type L | Medium | Residential, commercial, heating |
| Type K | Thickest | Underground, industrial |

#### Installation Notes

- Always use lead-free solder for potable water lines

- Clean pipe ends with emery cloth before soldering

- Apply flux thinly; excess flux causes corrosion inside the pipe

- Press-fit copper systems (no soldering) are gaining popularity; require proprietary fittings and press tools

## 2. Wire Types: BV vs BVR vs RVV

### Wire Type Comparison

| Wire Type | Full Name | Conductor Structure | Flexibility | Typical Use |
| --- | --- | --- | --- | --- |
| BV | Copper Core PVC Insulated | Single solid strand | Low (stiff) | Concealed in-wall wiring, fixed installation |
| BVR | Copper Core PVC Flexible | Multiple fine strands | Medium | Distribution cabinets, bending required areas |
| RVV | Copper Core PVC Flexible Sheathed | Multiple fine strands, sheathed | High | Appliances, extension cords, exposed runs |
| BVVB | Copper Core PVC Flat | Multiple parallel BV conductors | Low | Surface-mounted flat cable runs |
| RVVP | Shielded Flexible | Fine strands + braided shield | High | Audio, control, communication lines |

### Wire Gauge Selection by Circuit

| Circuit Type | Minimum Wire Size (mm²) | Wire Type | Breaker Rating |
| --- | --- | --- | --- |
| Lighting | 1.5 mm² | BV | 10A |
| General outlets (bedroom, living room) | 2.5 mm² | BV | 16A |
| Kitchen outlets | 4.0 mm² | BV | 20–25A |
| Air conditioner (1–1.5 HP) | 2.5 mm² | BV | 16A |
| Air conditioner (2–3 HP) | 4.0 mm² | BV | 25A |
| Central AC / instant water heater | 6.0 mm² | BV | 32A |
| Main entry (small apartment) | 10 mm² | BV | 40–50A |
| Main entry (large apartment) | 16 mm² | BV | 63A |

### Current Carrying Capacity (Copper, PVC, 25°C ambient)

| Wire Size (mm²) | Approx. Max Current (A) | Max Load (220V, kW) |
| --- | --- | --- |
| 1.5 | 15–18 | 3.3 |
| 2.5 | 22–25 | 5.5 |
| 4.0 | 32–38 | 8.3 |
| 6.0 | 40–48 | 10.5 |
| 10.0 | 55–65 | 14.3 |
| 16.0 | 75–85 | 18.7 |

Note: These are approximate values for single conductor in conduit. Actual capacity decreases with bundled conductors, higher ambient temperature, and longer runs. Always derate per local electrical codes.

## 3. Conduit Types: PVC vs Metal

### Comparison Table

| Feature | PVC Conduit (PVC电工管) | Metal Conduit (JDG/KBG/SC) |
| --- | --- | --- |
| Material | Rigid PVC | Galvanized steel (JDG, KBG) or black steel (SC) |
| Cost | Low | Moderate to high |
| Installation | Glue / solvent weld joints | Screw-type (JDG) or compression (KBG), threaded (SC) |
| Fire Resistance | Self-extinguishing (flame-retardant grade) | Excellent (non-combustible) |
| EMF Shielding | None | Good (metal provides shielding) |
| Corrosion Resistance | Excellent | Good (galvanized); SC requires additional protection |
| Bending | Requires heat bending or pre-formed elbows | Requires conduit bender (hand or hydraulic) |
| Common Use | Residential walls/ceilings | Commercial, fire-rated areas, exposed runs |
| Code Requirement | Acceptable for most residential | Required in some commercial/fire-rated constructions |

### PVC Conduit Specifications

| Nominal Diameter | Outer Diameter (mm) | Common Use |
| --- | --- | --- |
| 16mm | 16mm | Lighting circuits (1–2 wires) |
| 20mm | 20mm | Power circuits (2–3 wires) |
| 25mm | 25mm | Main runs, AC circuits |
| 32mm | 32mm | Service entry, bundle runs |

### Fill Ratio Rule

- Conduit must NOT be filled beyond 40% of cross-sectional area for 3+ conductors

- For 1–2 conductors: max 31% fill

- Example: A 20mm conduit can hold approximately 3 x 2.5mm² wires with earth

### Conduit Installation Checklist

- Use flame-retardant PVC conduit (marked with “阻燃” or flame rating)

- Maximum 2 bends (90°) between pull points / junction boxes

- Use large-radius bends — no kinks or crushed conduit

- Separate power and low-voltage (network/TV) conduits by at least 300mm

- Conduits in wet areas (bathroom) must be waterproof-sealed at entry points

- Label both ends of every conduit run before closing walls

- Leave pull string in every empty conduit for future use

- Metal conduit must be grounded (bonded) at both ends

## 4. Quick Reference: Material Selection by Scenario

| Renovation Scenario | Recommended Water Pipe | Recommended Wire | Conduit |
| --- | --- | --- | --- |
| Standard apartment renovation | PPR S2.5 (hot), S4 (cold) | BV | PVC |
| High-end / luxury | Copper Type L | BV (all) or BVR at panel | Metal (exposed), PVC (concealed) |
| Floor heating install | PEX-a for heating loops + PPR for supply | BV | PVC |
| Old building repipe | PEX (flexible, snakes through walls) | BVR (easier to pull) | PVC |
| Villa / multi-story | PPR S2.5 or copper | BV + RVVP for smart home | Mixed PVC + metal |
| Commercial space | Copper or PPR | BV | Metal (code required) |

## 5. Brand Recommendations

### Water Pipes

| Brand | Origin | Positioning | Notes |
| --- | --- | --- | --- |
| WAVE (伟星) | China | Mid–high | Widely available, good warranty |
| Rifeng (日丰) | China | Mid | Market leader, PEX-a specialist |
| LESSO (联塑) | China | Mid | Broad product range |
| Uponor | Finland | Premium | PEX-a gold standard |
| Viega | Germany | Premium | Copper and press-fit systems |

### Wire & Cable

| Brand | Origin | Notes |
| --- | --- | --- |
| Far East Cable (远东电缆) | China | Largest domestic manufacturer |
| Panda Wire (熊猫电线) | China | Trusted for residential BV wire |
| Baosheng (宝胜) | China | Industrial and residential |
| NKT | Denmark | Premium European quality |

### Conduit

| Brand | Notes |
| --- | --- |
| LESSO (联塑) | Full PVC conduit system |
| Zhongcai (中财) | Good value PVC |
| Generic JDG/KBG | Many manufacturers; verify galvanization quality |

# 装修材料采购清单（可勾选）

用途：全屋装修材料采购跟踪清单
适用阶段：全周期
文档版本：v1.0 | 最后更新：2026-05-16
使用说明：打印后逐项勾选，或在电子版中将 [ ] 改为 [x] 表示已采购

## 一、采购时间轴（按施工阶段）

| 阶段 | 时间节点 | 需采购材料 |
| --- | --- | --- |
| 开工前 | T-7天 | 水泥、沙子、红砖、防水材料 |
| 水电阶段 | 开工后1–3天 | 电线、水管、线管、底盒、配电箱、防水涂料 |
| 泥瓦阶段 | 水电验收后 | 墙砖、地砖、瓷砖胶、美缝剂、门槛石、窗台石 |
| 木作阶段 | 泥瓦验收后 | 柜体板材（工厂定制）、门（工厂定制）、石膏板、轻钢龙骨、木工板 |
| 油漆阶段 | 木作验收后 | 界面剂、腻子粉、乳胶漆、阴阳角条、网格布 |
| 安装阶段 | 油漆验收后 | 灯具、开关面板、洁具、橱柜、地板、集成吊顶、五金 |
| 软装阶段 | 竣工验收后 | 窗帘、家具、家电、装饰品 |

## 二、主材采购清单

### 2.1 瓷砖类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 客厅地砖 | 800×800 或 750×1500 | 优等品 / 吸水率≤0.5% | 同批次色差检查，多备5%损耗 | [ ] m² | [ ] | [ ] |
| 2 | 卧室地砖/地板 | 600×1200 或 地板 | 优等品 / E0级 | 如选地板确认E0级+耐磨转数 | [ ] m² | [ ] | [ ] |
| 3 | 厨房墙砖 | 300×600 或 400×800 | 优等品 | 耐油污釉面砖优先 | [ ] m² | [ ] | [ ] |
| 4 | 厨房地砖 | 同客厅或防滑砖 | 优等品 / 防滑系数R9以上 | 防滑等级至少R9 | [ ] m² | [ ] | [ ] |
| 5 | 卫生间墙砖 | 300×600 或 400×800 | 优等品 | 防水釉面，颜色建议浅色系 | [ ] m² | [ ] | [ ] |
| 6 | 卫生间地砖 | 300×300 防滑砖 | 优等品 / 防滑R10以上 | 坡度铺贴，防滑等级R10+ | [ ] m² | [ ] | [ ] |
| 7 | 阳台地砖 | 防滑砖 | 合格品以上 | 抗冻性（北方） | [ ] m² | [ ] | [ ] |
| 8 | 美缝剂/环氧彩砂 | / | 环保认证 / 低VOC | 德高/马贝/皇氏工匠，选与砖同色系 | [ ] 组 | [ ] | [ ] |

### 2.2 地板类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 强化复合地板 | 12mm厚度 | E0级 / 耐磨≥6000转 | 关注甲醛释放量+耐磨转数 | [ ] m² | [ ] | [ ] |
| 2 | 实木复合地板 | 15mm厚度 | E0级 / 三层/多层 | 表层实木厚度≥2mm | [ ] m² | [ ] | [ ] |
| 3 | 纯实木地板 | 18mm厚度 | E0级 | 含水率与当地平衡含水率匹配 | [ ] m² | [ ] | [ ] |
| 4 | 踢脚线 | 配套地板 | E0级 | 与地板同色系，PVC/实木/铝合金 | [ ] m | [ ] | [ ] |
| 5 | 防潮膜/地垫 | / | / | 2mm PE膜，铺地板前必备 | [ ] m² | [ ] | [ ] |

### 2.3 门窗类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 入户防盗门 | 2050×960mm | 甲级防盗 / 钢质 | C级锁芯、填充物、隔音条 | [1] 樘 | [ ] | [ ] |
| 2 | 卧室门（实木复合） | 2100×900mm | E0级 / 环保漆 | 关注隔音性能（≥30dB） | [ ] 樘 | [ ] | [ ] |
| 3 | 卫生间门 | 2100×800mm | 防潮 / 钛镁合金 | 磨砂/长虹玻璃，防潮防变形 | [ ] 樘 | [ ] | [ ] |
| 4 | 厨房门 | 定制尺寸 | / 铝合金+钢化玻璃 | 推拉门关注轨道/吊轨质量 | [1] 樘 | [ ] | [ ] |
| 5 | 窗户（断桥铝） | 定制尺寸 | 6063-T5铝材 / PA66隔热条 | 中空玻璃5+12A+5，五金件进口 | [ ] m² | [ ] | [ ] |
| 6 | 门锁/合页/门吸 | / | / | 304不锈钢，每门配2合页+1门吸 | [ ] 套 | [ ] | [ ] |

### 2.4 橱柜类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 地柜柜体 | 定制 | E0级 / 多层实木板 | 防潮板+阻尼铰链 | [ ] m | [ ] | [ ] |
| 2 | 吊柜柜体 | 定制 | E0级 / 多层实木板 | 承重挂件固定 | [ ] m | [ ] | [ ] |
| 3 | 台面（石英石） | 厚度≥15mm | 食品级 / 石英砂含量≥90% | 厚度15–20mm，无辐射检测报告 | [ ] m | [ ] | [ ] |
| 4 | 柜门 | 定制 | E0级 / 双饰面/PET | PET肤感膜/双饰面板，耐刮 | [ ] m² | [ ] | [ ] |
| 5 | 五金（铰链/滑轨） | / | / | 百隆/海蒂诗/DTC，全阻尼 | [ ] 套 | [ ] | [ ] |
| 6 | 拉篮/调味篮 | / | 304不锈钢 | 橱柜内功能配件 | [ ] 个 | [ ] | [ ] |
| 7 | 水槽+龙头 | 大单槽/双槽 | 304不锈钢 | 厚度≥0.8mm，抽拉龙头 | [1] 套 | [ ] | [ ] |

### 2.5 卫浴类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 马桶（连体/智能） | 坑距305/400mm | 节水型 / 一级水效 | 冲水量≤4L，智能选即热式 | [ ] 个 | [ ] | [ ] |
| 2 | 花洒套装 | 含顶喷+手持 | 节水型 / 铜主体 | 恒温款关注阀芯（陶瓷片） | [ ] 套 | [ ] | [ ] |
| 3 | 浴室柜 | 定制尺寸 | E0级 / 防潮板材 | 多层实木防潮板+陶瓷盆 | [ ] 套 | [ ] | [ ] |
| 4 | 镜柜/镜灯 | 定制 | / | 防雾镜+LED灯，镜柜深度150mm+ | [ ] 套 | [ ] | [ ] |
| 5 | 淋浴隔断 | 定制 | 钢化玻璃3C认证 | 8mm钢化玻璃+防爆膜 | [ ] m² | [ ] | [ ] |
| 6 | 地漏 | 100×100mm | 304不锈钢 | 深水封/磁悬浮防臭，淋浴区用长条 | [ ] 个 | [ ] | [ ] |
| 7 | 角阀 | 4分 | 铜质 / 陶瓷阀芯 | 冷热各1个，每卫至少4个 | [ ] 个 | [ ] | [ ] |
| 8 | 软管 | 长度按需 | 304不锈钢 | 耐压≥1.6MPa | [ ] 根 | [ ] | [ ] |
| 9 | 毛巾架/置物架 | / | 304不锈钢 / 太空铝 | 免打孔或打孔安装 | [ ] 套 | [ ] | [ ] |
| 10 | 浴霸/风暖 | 300×600mm | / | LED照明+换气+取暖，2600W以上 | [ ] 台 | [ ] | [ ] |

### 2.6 涂料类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 墙固/界面剂 | 18kg/桶 | 十环认证 | 基层处理必备，黄色墙固/绿色地固 | [ ] 桶 | [ ] | [ ] |
| 2 | 成品耐水腻子 | 20kg/袋 | JG/T 298标准 | 美巢800/立邦，不可用非成品腻子 | [ ] 袋 | [ ] | [ ] |
| 3 | 底漆 | 5L/18L | 十环认证 / VOC≤50g/L | 底漆不可省，防碱防霉 | [ ] 桶 | [ ] | [ ] |
| 4 | 面漆（乳胶漆） | 5L/18L | 十环+法国A+ / VOC≤50g/L | 一底两面，选哑光/丝光 | [ ] 桶 | [ ] | [ ] |
| 5 | 网格布/抗裂纤维网 | / | / | 新旧墙接缝/开槽处必备 | [ ] m² | [ ] | [ ] |
| 6 | 阴阳角条 | 2.5m/根 | PVC / 铝合金 | 墙角找直必备 | [ ] 根 | [ ] | [ ] |

### 2.7 吊顶类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 厨卫铝扣板吊顶 | 300×300/300×600 | 0.6mm以上厚度 | 防潮耐污，含安装龙骨 | [ ] m² | [ ] | [ ] |
| 2 | 客餐厅石膏板吊顶 | 1200×2400mm | 国标 / 防潮型 | 轻钢龙骨+9.5mm石膏板 | [ ] m² | [ ] | [ ] |
| 3 | 轻钢龙骨 | 38/50主龙骨 | 国标 / 镀锌 | 不使用木龙骨（潮湿区域） | [ ] m | [ ] | [ ] |
| 4 | 吊顶灯/筒灯 | / | LED | 色温3000K–4000K | [ ] 个 | [ ] | [ ] |

### 2.8 灯具类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 客厅主灯 | 直径600–800mm | LED / 显色指数Ra≥90 | 无频闪、低蓝光 | [1] 盏 | [ ] | [ ] |
| 2 | 餐厅灯 | / | LED / Ra≥90 | 餐桌上方2.1–2.2m高度 | [1] 盏 | [ ] | [ ] |
| 3 | 卧室灯 | 直径400–500mm | LED / 可调光 | 暖光2700–3000K | [ ] 盏 | [ ] | [ ] |
| 4 | 厨房灯 | 平板灯/吸顶灯 | LED / IP44 | 防潮，亮度充足 | [1] 盏 | [ ] | [ ] |
| 5 | 卫生间灯 | 防潮吸顶灯 | LED / IP44 | 防雾防潮 | [ ] 盏 | [ ] | [ ] |
| 6 | 筒灯/射灯 | / | LED / Ra≥90 | 色温统一3500–4000K | [ ] 个 | [ ] | [ ] |
| 7 | 灯带（灯槽） | / | LED / 低压24V | 磁吸轨道/嵌入式 | [ ] m | [ ] | [ ] |
| 8 | 开关插座面板 | 86型 | CCC认证 | 施耐德/西门子，五孔间距合理 | [ ] 个 | [ ] | [ ] |

## 三、辅材采购清单

### 3.1 水泥砂浆类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 水泥（P·O 42.5） | 50kg/袋 | 国标 GB 175 | 生产日期30天内，无结块 | [ ] 袋 | [ ] | [ ] |
| 2 | 中砂 | / | 含泥量≤3% | 河砂优先，不含杂质 | [ ] m³ | [ ] | [ ] |
| 3 | 瓷砖胶 | 20kg/袋 | JC/T 547标准 | 大砖上墙必须用瓷砖胶（C2级以上） | [ ] 袋 | [ ] | [ ] |
| 4 | 瓷砖背胶 | / | / | 大砖上墙必备，增强粘结力 | [ ] 桶 | [ ] | [ ] |
| 5 | 填缝剂 | 5kg/袋 | / | 过渡用，正式建议用美缝剂 | [ ] 袋 | [ ] | [ ] |

### 3.2 水电辅材类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 电线（BV 2.5mm²） | 100m/卷 | 国标 / CCC认证 | 远东/熊猫/正泰，阻燃型 | [ ] 卷 | [ ] | [ ] |
| 2 | 电线（BV 4mm²） | 100m/卷 | 国标 / CCC认证 | 空调/厨卫专用 | [ ] 卷 | [ ] | [ ] |
| 3 | 电线（BV 6mm²） | 100m/卷 | 国标 / CCC认证 | 大功率电器专用 | [ ] 卷 | [ ] | [ ] |
| 4 | 网线（六类） | 305m/箱 | 国标 / 无氧铜 | 秋叶原/康普/山泽，非铜包铝 | [ ] 箱 | [ ] | [ ] |
| 5 | PVC线管 | Φ16/Φ20 | 阻燃型 | 红蓝分色（强弱电分管） | [ ] 根 | [ ] | [ ] |
| 6 | 线管弯头/直接 | / | / | 86底盒配套 | [ ] 个 | [ ] | [ ] |
| 7 | 86暗盒 | / | 阻燃PVC | 深度≥50mm，带锁扣 | [ ] 个 | [ ] | [ ] |
| 8 | PPR水管（热水管） | Φ20/Φ25 | 国标 / S3.2系列 | 伟星/日丰/金德，热水管通用于冷热水 | [ ] 根 | [ ] | [ ] |
| 9 | PPR管件 | 弯头/三通/直接 | 同品牌 | 与水管同品牌，热熔连接 | [ ] 批 | [ ] | [ ] |
| 10 | 生料带 | / | / | 水管密封，至少2卷 | [ ] 卷 | [ ] | [ ] |
| 11 | 电工胶布 | / | / | 阻燃PVC胶布，多色 | [ ] 卷 | [ ] | [ ] |

### 3.3 防水类

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 防水涂料（JS） | 18kg/套 | 十环认证 / GB/T 23445 | 东方雨虹/德高，厨卫通用 | [ ] 套 | [ ] | [ ] |
| 2 | 聚氨酯防水涂料 | 10kg/桶 | 国标 / 环保型 | 柔性防水，地面优先 | [ ] 桶 | [ ] | [ ] |
| 3 | 堵漏王/水不漏 | 5kg/袋 | / | 管根/阴角密封处理 | [ ] 袋 | [ ] | [ ] |
| 4 | 无纺布/聚酯布 | / | / | 防水加强层（管根/阴角） | [ ] m² | [ ] | [ ] |

### 3.4 其他辅材

| 序号 | 材料名称 | 规格参考 | 环保/等级要求 | 采购要点 | 数量 | 预算 | 已购 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | 玻璃胶（防霉） | 支 | 环保型 / 中性硅酮 | 瓦克/GE/硅宝，厨卫用防霉型 | [ ] 支 | [ ] | [ ] |
| 2 | 发泡胶 | 支 | 环保型 | 门窗安装填缝 | [ ] 支 | [ ] | [ ] |
| 3 | 结构胶 | 支 | 环保型 | 台面/石材粘接 | [ ] 支 | [ ] | [ ] |
| 4 | 膨胀螺丝 | M6/M8 | 304不锈钢 | 吊柜/挂件安装 | [ ] 批 | [ ] | [ ] |
| 5 | 自攻螺丝 | / | / | 石膏板/木工固定 | [ ] 盒 | [ ] | [ ] |
| 6 | 美纹纸 | / | / | 刷漆保护/美缝辅助 | [ ] 卷 | [ ] | [ ] |
| 7 | 保护膜 | / | / | 成品保护（地面/门窗） | [ ] 卷 | [ ] | [ ] |

## 四、采购品牌参考

| 品类 | 经济型 | 舒适型 | 高端型 |
| --- | --- | --- | --- |
| 电线 | 正泰、德力西 | 远东、熊猫 | 宝胜、上上 |
| 水管 | 联塑、中财 | 伟星、日丰 | 皮尔萨、微法 |
| 防水 | 德高 | 东方雨虹、西卡 | 马贝、西卡 |
| 水泥 | 当地品牌 | 海螺、冀东 | 海螺、拉法基 |
| 乳胶漆 | 立邦净味120 | 多乐士、都芳 | 芬琳、佐敦、本杰明摩尔 |
| 瓷砖 | 冠珠、新中源 | 东鹏、马可波罗 | 诺贝尔、IMOLA |
| 洁具 | 法恩莎、恒洁 | 箭牌、TOTO | 科勒、杜拉维特 |
| 开关 | 公牛、正泰 | 施耐德、西门子 | 施耐德（高端系列） |
| 灯具 | 阳光照明 | 欧普、雷士 | 西顿、企一 |
| 五金 | DTC | 百隆基础款 | 百隆、海蒂诗、格拉斯 |

## 五、采购注意事项

- 主材提前量：定制类材料（橱柜/衣柜/门）需提前 25–40 天下单，生产周期长

- 批次一致性：瓷砖/地板/涂料同一次采购完毕，避免不同批次色差

- 验收再签收：瓷砖/地板到货先检查是否有破损、色差、型号不符

- 退换货条款：瓷砖/地板通常可退未泡水的整箱货，下单前确认退换政策

- 安装责任：明确谁负责安装（厂家安装/施工队安装），避免推诿

- 辅料不可忽视：玻璃胶、角阀、软管等小配件质量直接影响使用寿命

- 环保优先：所有与人直接接触的材料（板材、漆、胶水）优先选环保认证产品

# 装修材料选购指南

## 选购原则

- 环保优先

- 质量第一

- 价格适中

- 品牌保障

## 选购流程

- 确定预算

- 了解材料

- 对比品牌

- 实地考察

- 签订合同

## 选购技巧

### 瓷砖

- 看平整度

- 听声音

- 试吸水率

- 测防滑性

### 地板

- 看环保等级

- 检查含水率

- 测试耐磨性

### 涂料

- 看环保标识

- 闻气味

- 查检测报告

### 卫浴

- 看釉面

- 检查水件

- 确认配件

## 选购渠道

| 渠道 | 优点 | 缺点 |
| --- | --- | --- |
| 建材市场 | 可看实物 | 价格不透明 |
| 品牌店 | 品质保障 | 价格高 |
| 电商 | 价格透明 | 无法看实物 |

# 密封材料指南 (Sealant Materials Guide)

## 概述

密封材料在装修中扮演着防水、防漏、隔音、美观的重要角色。从卫生间防水到门窗密封，从瓷砖填缝到管道封堵，选择合适的密封材料直接关系到装修质量和使用寿命。

## 密封胶分类与选型

### 硅胶密封胶（硅酮密封胶）

#### 类型对比

| 类型 | 特点 | 适用场景 | 不适用场景 | 参考单价（元/支） |
| --- | --- | --- | --- | --- |
| 酸性硅胶 | 固化快、粘接力强、有刺激性气味 | 玻璃、陶瓷、金属 | 水泥、石材、碱性材料 | 10–30 |
| 中性硅胶 | 无腐蚀、适用面广 | 几乎所有材料 | 潮湿环境固化慢 | 15–50 |
| 防霉硅胶 | 添加防霉剂 | 卫生间、厨房、水槽 | 户外长期暴晒 | 20–60 |
| 耐候硅胶 | 抗 UV、耐温变 | 门窗密封、幕墙 | 室内潮湿环境 | 25–80 |
| 结构硅胶 | 高强度、高弹性 | 玻璃幕墙、阳光房 | 一般家装 | 40–150 |

#### 技术参数

| 参数 | 酸性硅胶 | 中性硅胶 | 防霉硅胶 | 耐候硅胶 |
| --- | --- | --- | --- | --- |
| 固化时间（表干） | 10–30 分钟 | 30–60 分钟 | 30–60 分钟 | 30–60 分钟 |
| 完全固化 | 24 小时 | 48–72 小时 | 48–72 小时 | 48–72 小时 |
| 使用温度 | -40 至 150 度 C | -40 至 150 度 C | -40 至 150 度 C | -50 至 200 度 C |
| 位移能力 | +/- 25% | +/- 25% | +/- 20% | +/- 25% |
| 使用寿命 | 10–15 年 | 15–20 年 | 5–10 年 | 20–25 年 |

#### 品牌推荐

| 品牌 | 产地 | 特点 | 适合产品线 |
| --- | --- | --- | --- |
| 道康宁（Dow） | 美国 | 行业标杆 | 全系列 |
| 瓦克（Wacker） | 德国 | 品质稳定 | GENIOSIL 系列 |
| 白云 | 中国 | 性价比高 | 中性防霉系列 |
| 之江 | 中国 | 国产一线 | JS 系列 |
| 硅宝 | 中国 | 工程常用 | 家装系列 |

### 聚氨酯密封胶（PU 密封胶）

#### 特点与应用

| 特性 | 说明 |
| --- | --- |
| 粘接性 | 对混凝土、金属、木材粘接极佳 |
| 弹性 | 伸长率 300%–600% |
| 耐磨性 | 优于硅胶，适合地面伸缩缝 |
| 可涂覆性 | 表面可刷漆 |
| 固化方式 | 湿气固化 |
| 耐候性 | 中等，不推荐长期暴晒环境 |

#### 适用场景

| 场景 | 推荐型号 | 原因 |
| --- | --- | --- |
| 混凝土伸缩缝 | 聚氨酯单组分 | 粘接混凝土好、弹性佳 |
| 屋面防水 | 聚氨酯密封胶 | 耐水性好、可涂覆 |
| 地下室防水 | 聚氨酯密封胶 | 耐水压 |
| 地板伸缩缝 | 聚氨酯柔性胶 | 耐磨、可上漆 |
| 外墙接缝 | 不推荐 | 耐候性不足 |

#### 品牌推荐

| 品牌 | 参考单价（元/支） | 特点 |
| --- | --- | --- |
| 西卡（Sika） | 40–120 | 全球领先，品质保障 |
| 马贝（Mapei） | 50–150 | 建材领域专业品牌 |
| 三棵树 | 20–60 | 国产性价比 |

### 丁基密封胶带（Butyl Tape）

#### 特点

| 特性 | 说明 |
| --- | --- |
| 材质 | 丁基橡胶 + 填料 |
| 形态 | 胶带状（卷材） |
| 粘性 | 永久不干，自粘性极强 |
| 耐温 | -40 至 90 度 C |
| 寿命 | 20 年以上 |
| 施工 | 撕开隔离纸直接粘贴 |

#### 应用场景

| 场景 | 使用方法 | 效果 |
| --- | --- | --- |
| 门窗安装密封 | 贴于窗框与墙体接缝处 | 防水、隔音 |
| 管道穿墙密封 | 包裹管道后嵌入墙体 | 防水、防虫 |
| 屋面防水 | 铺设于接缝处 | 辅助防水 |
| 阳光房密封 | 玻璃与框架之间 | 防水密封 |
| 彩钢板搭接 | 板缝间铺设 | 防渗漏 |

#### 规格选择

| 规格 | 适用场景 |
| --- | --- |
| 10mm x 3mm | 细缝密封 |
| 20mm x 3mm | 门窗密封 |
| 20mm x 5mm | 管道密封 |
| 50mm x 3mm | 屋面防水 |

### 发泡密封胶（聚氨酯发泡胶）

#### 类型

| 类型 | 膨胀率 | 适用缝隙宽度 | 特点 |
| --- | --- | --- | --- |
| 枪式发泡胶 | 60–80 倍 | 10–50mm | 施工精准、用量可控 |
| 管式发泡胶 | 50–70 倍 | 5–30mm | 操作简便、适合小量 |
| 阻燃型发泡胶 | 60 倍 | 10–50mm | 氧指数 >= 26，防火 |
| 低温型发泡胶 | 50–60 倍 | 10–50mm | 0 度 C 以下可用 |

#### 性能参数

| 参数 | 标准值 |
| --- | --- |
| 密度 | 20–35 kg/m3 |
| 导热系数 | 0.03–0.04 W/(m.K) |
| 抗拉强度 | >= 60 kPa |
| 延伸率 | >= 5% |
| 隔音量 | 20–30 dB |
| 使用寿命 | 15–20 年 |

#### 施工要点

- 缝隙清理干净，无灰尘、油污

- 轻微湿润缝隙表面（发泡胶需要湿气固化）

- 填充量控制在缝隙体积的 2/3（发泡会膨胀）

- 固化后用刀切除多余部分

- 表面用密封胶或水泥砂浆覆盖（发泡胶不耐 UV）

#### 品牌推荐

| 品牌 | 参考单价（元/支） | 特点 |
| --- | --- | --- |
| 速的奥（Soudal） | 25–60 | 欧洲品牌，品质优良 |
| 桑莱斯（Sunrise） | 20–50 | 国内一线 |
| 东方雨虹 | 15–40 | 国产性价比 |
| 三棵树 | 15–35 | 性价比高 |

## 选材对照表

### 按场景选材

| 使用场景 | 推荐材料 | 替代方案 | 不推荐 |
| --- | --- | --- | --- |
| 卫生间洁具密封 | 中性防霉硅胶 | – | 酸性硅胶 |
| 厨房台面密封 | 中性防霉硅胶 | 丁基胶带 | – |
| 门窗框与墙体 | 发泡胶 + 外墙硅胶 | 丁基胶带 | 酸性硅胶 |
| 玻璃与金属框 | 中性硅胶或结构胶 | – | 发泡胶 |
| 瓷砖填缝 | 环氧填缝剂/美缝剂 | 硅胶（临时） | 发泡胶 |
| 管道穿墙 | 发泡胶 + 丁基胶带 | 防火泥 | – |
| 屋面伸缩缝 | 聚氨酯密封胶 | – | 硅胶 |
| 地板伸缩缝 | 聚氨酯密封胶 | – | 硅胶 |
| 阳光房顶密封 | 耐候硅胶 | 结构硅胶 | 普通硅胶 |
| 地下室变形缝 | 聚氨酯密封胶 | 遇水膨胀止水条 | 硅胶 |

## 施工注意事项

### 通用施工要求

| 项目 | 要求 |
| --- | --- |
| 基层处理 | 清洁、干燥（除发泡胶外）、无油污 |
| 施工温度 | 5–35 度 C（具体看产品说明） |
| 施工湿度 | 40%–70%（湿度过高影响固化） |
| 胶缝宽度 | 一般为 3–20mm |
| 胶缝深度 | 宽度的一半（使用背衬棒控制） |
| 三面粘接 | 避免，应使用背衬棒实现两面粘接 |

### 施工步骤（以硅胶为例）

- 清理：用酒精或专用清洁剂清洗基材表面

- 贴美纹纸：胶缝两侧贴美纹纸，确保边缘整齐

- 装胶枪：将胶管装入胶枪，45 度角切割胶嘴

- 打胶：匀速打胶，确保胶体填满缝隙

- 刮平：用刮板或手指（蘸水）刮平胶面

- 撕纸：在表干前撕去美纹纸

- 养护：固化期间避免触碰和水淋

### 质量检验

| 检验项目 | 合格标准 | 检验方法 |
| --- | --- | --- |
| 外观 | 表面平整光滑、无气泡、无裂缝 | 目视检查 |
| 粘接 | 与两侧基材粘接牢固 | 手拉试验 |
| 宽度 | 偏差在 +/- 1mm 内 | 卡尺测量 |
| 固化 | 完全固化后无粘性 | 手指触摸 |
| 防水 | 淋水试验无渗漏 | 淋水试验 |

## 密封材料寿命与维护

### 使用寿命

| 材料 | 室内寿命 | 室外寿命 | 卫生间/厨房寿命 |
| --- | --- | --- | --- |
| 中性硅胶 | 15–20 年 | 10–15 年 | 3–5 年（防霉型） |
| 酸性硅胶 | 10–15 年 | 8–10 年 | 2–3 年 |
| 聚氨酯密封胶 | 10–15 年 | 5–8 年 | 不推荐 |
| 丁基胶带 | 20 年以上 | 15–20 年 | 20 年以上 |
| 发泡胶 | 15–20 年 | 5–10 年（需覆盖） | 不直接暴露 |

### 维护建议

| 场景 | 维护周期 | 维护方法 |
| --- | --- | --- |
| 卫生间硅胶 | 每 2–3 年 | 铲除旧胶、清理、重新打胶 |
| 门窗密封胶 | 每 5 年检查 | 发现开裂及时修补 |
| 厨房台面胶 | 每 2–3 年 | 清除污渍，检查是否脱胶 |
| 屋面密封胶 | 每 3–5 年 | 全面检查，更换老化胶缝 |
| 发泡胶 | 每 5 年 | 检查是否粉化，必要时重新填充 |

## 常见问题

| 问题 | 原因 | 处理方法 |
| --- | --- | --- |
| 胶体开裂 | 位移超出胶的弹性范围 | 铲除重打，选用更高位移能力的胶 |
| 粘接不牢 | 基层未清理或有油污 | 重新清理后施工 |
| 表面发粘不固化 | 温度过低或湿度不够 | 改善环境条件 |
| 变色 | UV 照射或材质问题 | 选用耐候型或防变色产品 |
| 发霉 | 环境潮湿、未用防霉型 | 铲除后重新打防霉硅胶 |
| 脱落 | 三面粘接 | 使用背衬棒，确保两面粘接 |

# 智能家居材料预埋指南 (Smart Home Pre-installation Guide)

## 1. Why Pre-installation Matters

Smart home retrofitting after renovation is expensive, messy, and often aesthetically compromised. Proper pre-installation during renovation ensures clean wire management, reliable connections, and future-proofing. This guide covers conduit planning, wiring, sensor positioning, and infrastructure requirements.

### Renovation Phase Checklist

| Phase | Smart Home Tasks |
| --- | --- |
| Design | Select ecosystem, map device locations, plan network topology |
| Demolition | Mark new outlet locations, identify hub placement |
| Electrical rough-in | Run neutral wires to all switch locations, install extra conduits |
| Low-voltage rough-in | Network cables, sensor wires, speaker wires, security |
| Wall closing | Photograph all wire runs, label both ends, test continuity |
| Finishing | Install smart switches, sensors, hubs, APs |
| Commissioning | Network setup, device pairing, automation programming |

## 2. Smart Home Ecosystem Selection

### Platform Comparison

| Ecosystem | Protocol | Local Control | Hub Required | Voice Assistant | Notes |
| --- | --- | --- | --- | --- | --- |
| Apple HomeKit | Thread, Wi-Fi, Bluetooth | Yes (with Thread Border Router) | Apple TV / HomePod / HomePod mini | Siri | Premium, privacy-focused, best iOS integration |
| Xiaomi / Mi Home (米家) | Zigbee 3.0, BLE Mesh, Wi-Fi | Partial (depends on device) | Xiaomi Gateway / Multimode | Xiao Ai | Widest device selection in China, cost-effective |
| Aqara | Zigbee 3.0, Thread, Wi-Fi | Yes (with Aqara Hub M2/M3) | Aqara Hub M2/M3 | Siri, Alexa, Google | Good HomeKit support, quality hardware |
| Tuya / Smart Life | Wi-Fi, Zigbee | Partial | Tuya Gateway | Alexa, Google | Massive device compatibility, budget |
| Home Assistant | Zigbee, Z-Wave, Thread, Wi-Fi, MQTT | Yes (fully local) | HA server (Raspberry Pi / NAS) | Any | Ultimate flexibility, DIY, technical skill needed |
| Huawei HiLink (鸿蒙) | Wi-Fi, BLE, PLC | Yes | Huawei router / hub | Celia | Growing ecosystem, PLC wired reliability |

### Protocol Comparison

| Protocol | Range | Bandwidth | Power Use | Mesh | Best For |
| --- | --- | --- | --- | --- | --- |
| Zigbee 3.0 | 10–30m indoor | 250 kbps | Very low | Yes | Sensors, switches, locks |
| Z-Wave | 30–100m indoor | 100 kbps | Very low | Yes | Sensors, locks, thermostats |
| Thread | 10–30m indoor | 250 kbps | Very low | Yes | Next-gen standard, Matter compatible |
| Wi-Fi | 30–50m indoor | 100+ Mbps | High | No | Cameras, displays, speakers |
| Bluetooth LE / BLE Mesh | 10m | 1–2 Mbps | Low | Yes (mesh) | Proximity sensors, remotes |
| Matter (over Thread/Wi-Fi) | Depends on underlying | Varies | Varies | Yes | Universal standard (future-proof) |
| RS-485 (wired) | 1000m+ | High | N/A | No | Commercial, wired reliability |

Recommendation: Plan for Zigbee 3.0 or Thread for sensors and switches, Wi-Fi for cameras and displays, and ensure your hub supports Matter for future compatibility.

## 3. Conduit Pre-Planning (管道预埋)

### General Rules

- Every switch box needs a neutral wire — this is the single most important pre-installation rule

- Run at least one extra empty conduit to each major location for future expansion

- Use 20mm conduits (not 16mm) for switch locations to allow future cable additions

- Separate power and low-voltage conduits by minimum 300mm

### Conduit Layout by Room

#### Living Room

| Location | Conduits Needed | Wire Types | Notes |
| --- | --- | --- | --- |
| TV wall | 3 x 20mm conduits | Power + HDMI/ethernet + spare | HDMI conduit with pull string |
| Sofa wall | 2 x 20mm conduits | Power + ethernet | For floor lamp + smart speaker |
| Ceiling center | 2 x 20mm conduits | Power (ceiling light) + neutral | Smart switch needs neutral |
| Corner (curtain) | 1 x 20mm conduit | Power at ceiling height | For motorized curtain track |
| Window (sensor) | 1 x 16mm spare | Optional wired contact sensor | Usually wireless is sufficient |

#### Kitchen

| Location | Conduits Needed | Wire Types | Notes |
| --- | --- | --- | --- |
| Under-sink | 2 x 20mm | Power + spare | Water purifier, leak sensor, garbage disposal |
| Above cooktop | 1 x 20mm | Power | Smart range hood |
| Countertop level | 2 x 20mm | Power | Smart appliance outlets |
| Ceiling | 1 x 20mm | Power | Smart light / gas detector |
| Fridge area | 1 x 20mm | Power (dedicated circuit) | Smart fridge |

#### Bedroom

| Location | Conduits Needed | Wire Types | Notes |
| --- | --- | --- | --- |
| Each side of bed | 2 x 20mm | Power + USB | Bedside outlets + smart lamp |
| Door | 2 x 20mm | Power (switch) + neutral | Smart switch + scene panel |
| Window | 1 x 16mm | Power (optional) | Motorized curtain/blind |
| Ceiling | 2 x 20mm | Power + neutral | Smart light + optional projection screen power |

#### Bathroom

| Location | Conduits Needed | Wire Types | Notes |
| --- | --- | --- | --- |
| Mirror area | 2 x 20mm | Power | Smart mirror, LED lighting |
| Ceiling | 2 x 20mm | Power | Smart exhaust fan, heater, light |
| Toilet area | 1 x 20mm | Power | Smart toilet seat |
| Shower area | 1 x 16mm | Power (IP-rated) | Digital shower controller (optional) |
| Wall (sensor) | 1 x 16mm spare | Optional wired humidity sensor | Usually wireless |

### Switch Box Requirements

| Switch Type | Box Size | Wiring Needed |
| --- | --- | --- |
| Standard single gang | 86 x 86mm | Live + Neutral + Load (each way) |
| Multi-gang (2–3 gang) | 86 x 86mm (deep) | Live + Neutral + multiple loads |
| Scene panel / touchscreen | 86 x 86mm (deep 50mm+) | Live + Neutral + ethernet (recommended) |
| Curtain switch | 86 x 86mm | Live + Neutral + 2 switched legs |
| Dimmer switch | 86 x 86mm (deep) | Live + Neutral + Load + earth |

Critical: Request electricians to run neutral wire (零线) to EVERY switch location. Traditional Chinese wiring often omits neutral at switches (switch only breaks live). Smart switches need both live and neutral to power their electronics.

## 4. Wiring for Smart Switches

### Smart Switch Wiring Diagram (Text)

Distribution Box
    |
    |--- Live (火线) --------------------+--- to smart switch L terminal
    |                                     |
    |--- Neutral (零线) ------------------+--- to smart switch N terminal
    |
    +--- Earth (地线) --------------------+--- to smart switch E terminal (if metal)

Smart Switch
    |
    +--- L1, L2, L3 (load wires) -----> to each light fixture

### Wire Requirements

| Connection | Wire Size | Type | Notes |
| --- | --- | --- | --- |
| Live to switch | 2.5mm² | BV | Standard |
| Neutral to switch | 2.5mm² | BV | Must be added if not present |
| Load wires (to lights) | 1.5–2.5mm² | BV | Per lighting circuit |
| Earth | 2.5mm² | BVR | Required for metal switch plates |

### Smart Switch Types

| Type | Neutral Required | Installation | Best For |
| --- | --- | --- | --- |
| Zero-fire version (零火版) | Yes | L + N + Load | New construction, renovation (preferred) |
| Single-fire version (单火版) | No | L + Load only | Retrofit (existing homes), but less reliable |
| No-neutral version (无零线) | No | L + Load | Last resort; requires bypass capacitor |

Always choose zero-fire version (零火版) for new installations. Single-fire switches have issues with low-wattage LED flickering and are less reliable.

## 5. Sensor Mounting Positions

### Sensor Placement Guide

| Sensor Type | Recommended Height | Location | Spacing | Notes |
| --- | --- | --- | --- | --- |
| Motion (PIR) | 2.2–2.5m | Ceiling corner, facing entry | 5–8m coverage radius | Avoid pointing at AC vents, windows |
| Motion (mmWave) | 2.5–3.0m | Ceiling center of room | 6m coverage radius | Detects presence (breathing), not just motion |
| Door/Window Contact | Door frame height | Top corner of door/window | One per door/window | Magnet on door, sensor on frame |
| Temperature/Humidity | 1.5m | Interior wall, shaded | One per zone/room | Away from direct sun, AC vents, kitchens |
| Light (Lux) | 1.5m | Interior wall | One per room | Away from direct lamp light |
| Water Leak | Floor level | Under sinks, near water heater, washing machine | One per wet area | Place on lowest point |
| Smoke Detector | Ceiling center | Each room, hallway | Per fire code | Interconnected if wired |
| Gas Detector | Ceiling (natural gas) or floor (LPG) | Kitchen, near gas appliance | One per gas appliance area | Natural gas rises; LPG sinks |
| Air Quality (VOC/PM2.5) | 1.5m | Living room, bedroom | One per floor | Away from kitchen, open windows |
| Noise | 1.5m | Living room, nursery | One per room | For automation triggers |

### mmWave Sensor vs PIR

| Feature | PIR (Passive Infrared) | mmWave (Millimeter Wave Radar) |
| --- | --- | --- |
| Detection | Body heat movement | Micro-movement (breathing, typing) |
| “Still person” detection | No (turns off if sitting still) | Yes (detects presence even when still) |
| Through materials | No (line of sight) | Yes (through thin walls, glass, fabric) |
| False triggers | Moderate (pets, sunlight) | Low |
| Cost | ¥20–80 | ¥80–300 |
| Power | Battery or wired | Wired (5V or 12V) |
| Recommended Use | Hallways, entry, closets | Living rooms, bedrooms, bathrooms |

### mmWave Sensor Installation Checklist

- Mount on ceiling for best coverage (360° models)

- Wall mount at 2.5m+ if ceiling not possible (directional models)

- Power: run 5V USB-C or 12V DC wire to sensor location

- Avoid placing near rotating fans, curtains, or moving objects that trigger false detection

- Configure detection zone in software to exclude false trigger areas

- Set appropriate “unoccupied delay” (30–60 seconds recommended)

## 6. Network Cable Requirements

### Cable Category Selection

| Cable Category | Max Speed | Max Distance | Suitable For | Recommendation |
| --- | --- | --- | --- | --- |
| Cat 5e | 1 Gbps | 100m | Basic internet | Minimum — avoid for new installs |
| Cat 6 | 1–10 Gbps | 55m (10G) / 100m (1G) | Gigabit + future | Recommended for most homes |
| Cat 6a | 10 Gbps | 100m | 10G backbone, PoE++ | Ideal for future-proofing |
| Cat 7 | 10 Gbps | 100m | Shielded installations | Overkill for most; harder to terminate |
| Cat 8 | 40 Gbps | 30m | Data centers | Unnecessary for residential |

Recommendation: Install Cat 6a (六类a) to all fixed locations. The cost difference from Cat 6 is minimal during construction, and it supports 10 Gbps for future network upgrades.

### Network Drop Points

| Location | Number of Cat 6a Drops | Notes |
| --- | --- | --- |
| TV wall | 3–4 | TV, set-top box, game console, spare |
| Each bedroom | 2 | Desktop PC, spare |
| Study / office | 4–6 | Desktop, NAS, printer, monitor, spare |
| Kitchen | 1 | Smart display / tablet |
| Living room ceiling | 1 | Wi-Fi AP (ceiling mount) |
| Each floor hallway | 1 | Wi-Fi AP |
| Distribution box | As needed | Smart home hub, network switch |
| Door entrance | 1 | Smart doorbell / camera |
| Balcony | 1 | Security camera |
| Garage | 1 | EV charger communication (optional) |

### PoE (Power over Ethernet) Devices

| Device | PoE Standard | Power | Notes |
| --- | --- | --- | --- |
| IP Camera | 802.3af (PoE) | 15.4W | Most common |
| Wi-Fi AP (ceiling) | 802.3af (PoE) | 15.4W | Ubiquiti, TP-Link Omada |
| Smart doorbell | 802.3af (PoE) | 15.4W | Wired alternative to battery |
| IP Phone | 802.3af (PoE) | 15.4W | Optional for home |
| PoE Switch | 802.3at (PoE+) | 30W | For downstream devices |
| Smart display | 802.3at (PoE+) | 30W | Wall-mounted control panel |

### Network Topology Recommendation

Internet (fiber optic modem / ONT)
    |
    |--- Main Router (with 2.5G WAN port)
            |
            +--- 2.5G/10G Switch (in distribution box)
                    |
                    +--- Cat 6a to each room drop
                    +--- Cat 6a to ceiling APs
                    +--- Cat 6a to PoE cameras
                    +--- Cat 6a to smart home hub
                    +--- Cat 6a to NAS

### Network Installation Checklist

- Run minimum Cat 6a, solid copper (not CCA — Copper-Clad Aluminum)

- Use shielded cable (STP) only if running near power lines; otherwise UTP is fine

- Label both ends of every cable

- Test every cable with certification tester (Fluke or equivalent)

- Leave 1m service loop at both ends

- Use structured media enclosure / patch panel in distribution box

- Conduit size: minimum 20mm for network cable runs (allow for future re-pull)

- Do NOT run network and power in the same conduit

## 7. Central Hub Placement

### Hub Placement Criteria

| Factor | Requirement | Why |
| --- | --- | --- |
| Centrality | Central location in home | Maximizes Zigbee/Thread range to all devices |
| Elevation | 1.5–2.0m height | Avoids floor-level obstruction |
| Power | Always-on outlet (not switched) | Hub must run 24/7 |
| Network | Ethernet connection (not Wi-Fi) | Reliable, low-latency backbone |
| Ventilation | Open area, not enclosed in metal box | Zigbee/Thread signals attenuate in metal enclosures |
| Accessibility | Accessible for maintenance | USB ports, reset buttons, SD cards |

### Recommended Hub Locations

| Home Type | Best Hub Location | Notes |
| --- | --- | --- |
| Small apartment (1–2 BR) | Living room shelf or TV cabinet | Central, easy access |
| Large apartment (3+ BR) | Central hallway ceiling or utility room | Maximize radio range |
| Multi-story villa | Each floor has a hub, wired together | Zigbee doesn’t cross floors well |
| With NAS | Next to NAS / in equipment rack | Consolidate infrastructure |
| With HomeKit | Near Apple TV / HomePod | Thread Border Router co-location |

### Equipment Rack / Distribution Box Setup

| Component | Size / Space | Notes |
| --- | --- | --- |
| Router | 1U or desktop | 2.5G WAN minimum |
| Switch | 8–16 port PoE+ | Managed switch with VLAN support |
| Smart Home Hub | Desktop (15 x 15 x 5cm) | Aqara M3, Home Assistant, etc. |
| NVR (camera recorder) | 4–8 bay | If using wired cameras |
| NAS | 2–4 bay | Media, backups, Home Assistant |
| Patch panel | 12–24 port | Organize all network drops |
| UPS | 600–1500VA | Keep network running during outages |
| Enclosure | 400 x 300 x 120mm minimum | Ventilated metal or plastic cabinet |

### Equipment Rack Checklist

- Dedicated 16A circuit for network equipment

- UPS backup for router, switch, and hub

- Ventilation: minimum 2 fans or passive vents

- Cable management: velcro ties (not zip ties) for serviceability

- Label every cable at both ends

- Leave 30% spare ports on switch for future devices

- Configure VLANs: separate IoT devices from main network

- Document IP addresses and device assignments

## 8. Special Considerations

### Smart Curtain Pre-installation

| Curtain Type | Power Location | Conduit | Notes |
| --- | --- | --- | --- |
| Motorized track | Ceiling, end of curtain rod | 20mm conduit to one end | Measure track length + 15cm for motor |
| Roller blind | Ceiling or wall, top of window | 16mm conduit | Battery options available |
| Venetian blind | Wall, beside window | 16mm conduit | Smart tilt/raise control |
| Roman shade | Ceiling | 16mm conduit | Requires compatible motor |

### Smart Lock Pre-installation

| Door Type | Requirement | Notes |
| --- | --- | --- |
| Wooden door | Standard mortise size (6068 or 7255) | Measure before purchasing lock |
| Metal security door | Confirm lock body compatibility | May need adapter plate |
| Double door | Confirm latch direction | Smart locks are handed |
| Glass door | Special glass door lock | Different mechanism |

Tip: No wiring needed for smart locks (battery powered), but consider pre-running a low-voltage wire for future hardwired models.

### Smart Mirror / Bathroom TV

| Item | Power Location | Water Protection |
| --- | --- | --- |
| Smart mirror | Above mirror, concealed | IP44 minimum |
| Bathroom TV | Above vanity or in niche | IP65 for shower-adjacent areas |
| Heated towel rack | Wall, beside shower | Dedicated 16A circuit |

### Projector Pre-installation

| Item | Requirement | Notes |
| --- | --- | --- |
| Ceiling mount | Reinforced ceiling box or concrete anchor | Verify projector weight capacity |
| HDMI conduit | 25mm conduit from TV rack to projector | HDMI 2.1 requires high-quality cable |
| Power | 1 x 10A outlet at projector location |  |
| Screen power | 1 x 10A outlet at screen location | For motorized screen |
| Speaker wire | 2 x 16mm² to rear speaker locations | If planning surround sound |

## 9. Complete Pre-installation Checklist

### Electrical

- Neutral wire at EVERY switch location

- 20mm conduits at all switch boxes (not 16mm)

- Extra empty conduit to major locations

- Dedicated circuit for smart water heater

- Outlet under every sink (water purifier, leak sensor)

- Outlet at ceiling for motorized curtains

- Outlet at door entrance for smart doorbell/camera

### Low-Voltage

- Cat 6a to every room (minimum 2 drops per room)

- Cat 6a to TV wall (3–4 drops)

- Cat 6a to ceiling AP locations

- Cat 6a to smart home hub location

- Cat 6a for doorbell camera

- Cat 6a for each PoE camera location

- Spare conduits with pull string everywhere

### Structural

- Reinforced ceiling mount for projector

- Reinforced wall for wall-mounted smart display

- Niche in shower for smart controls

- Equipment rack / cabinet space in distribution area

- Ventilation plan for equipment rack

### Final Verification (Before Wall Closing)

- Photograph every wall with conduits visible

- Label both ends of every wire and conduit

- Test continuity of all network cables

- Test power to all outlet locations

- Verify neutral present at all switch boxes

- Document smart device plan with exact locations

- Share documentation with future self / next electrician

## 10. Cost Estimates

### Pre-installation Cost Breakdown

| Item | Unit Cost | Typical Quantity | Total |
| --- | --- | --- | --- |
| Extra neutral wire to switches | ¥5–10/m | 50–100m | ¥250–1000 |
| Extra empty conduit (20mm) | ¥3–5/m | 30–50m | ¥90–250 |
| Cat 6a cable | ¥2–4/m | 200–400m | ¥400–1600 |
| Network outlet (faceplate + module) | ¥15–30/point | 10–20 points | ¥150–600 |
| Smart switch (zero-fire, per gang) | ¥50–150 | 10–20 switches | ¥500–3000 |
| Smart home hub | ¥200–800 | 1–2 | ¥200–1600 |
| Wi-Fi AP (ceiling, PoE) | ¥200–600 | 2–4 | ¥400–2400 |
| PoE switch (8-port) | ¥300–800 | 1 | ¥300–800 |
| Estimated total (pre-installation materials) |  |  | ¥2290–11250 |

Note: These are material costs only. Labor for extra wiring during renovation typically adds 20–40%. The cost of retrofitting after renovation (chasing walls, surface-mount trunking) can be 3–5x higher.

## 11. Common Mistakes to Avoid

| Mistake | Consequence | Prevention |
| --- | --- | --- |
| No neutral at switches | Cannot install reliable smart switches | Specify “零线到每个开关” to electrician |
| 16mm conduit at switches | Cannot pull additional wires later | Use 20mm minimum |
| No spare conduit | No room for future upgrades | Always run 1 extra empty conduit |
| Cat 5e instead of Cat 6a | Limited to 1 Gbps, no 10G future | Specify Cat 6a minimum |
| Hub in metal cabinet | Zigbee/Thread signal blocked | Use plastic/vented enclosure |
| No network to ceiling | Cannot install ceiling AP | Plan AP locations early |
| No outlet under sink | Cannot power leak sensor/purifier | Add under-sink outlets |
| No curtain motor power | Cannot add motorized curtains later | Run power to curtain track end |
| Wi-Fi hub instead of Ethernet hub | Unreliable smart home network | Hub on wired Ethernet |
| No equipment rack documentation | Future electricians can’t trace wires | Label and photograph everything |

# 瓷砖种类详解

## 按材质分类

| 类型 | 特点 | 适用场景 |
| --- | --- | --- |
| 抛光砖 | 表面光亮、硬度高 | 客厅地面 |
| 釉面砖 | 花色丰富、防滑 | 厨卫墙地面 |
| 通体砖 | 正反面一致、耐磨 | 阳台、走廊 |
| 玻化砖 | 吸水率低、硬度高 | 客厅地面 |
| 马赛克 | 装饰性强 | 背景墙 |

## 按用途分类

| 类型 | 特点 | 适用场景 |
| --- | --- | --- |
| 地砖 | 防滑、耐磨 | 地面 |
| 墙砖 | 轻薄、美观 | 墙面 |
| 厨卫砖 | 防水、防滑 | 厨卫 |
| 户外砖 | 耐候、防滑 | 阳台、花园 |

## 选购要点

- 看表面是否平整

- 听声音是否清脆

- 试吸水率是否达标

- 测防滑性是否合格

# 瓷砖选购详解

## 瓷砖分类

| 类型 | 特点 | 适用场景 |
| --- | --- | --- |
| 抛光砖 | 光亮、硬度高 | 客厅地面 |
| 釉面砖 | 花色丰富 | 厨卫墙面 |
| 通体砖 | 正反面一致 | 阳台 |
| 仿古砖 | 复古风格 | 美式风格 |
| 木纹砖 | 仿真木地板 | 卧室 |
| 大理石瓷砖 | 仿真大理石 | 客厅地面 |
| 岩板 | 大规格、薄 | 背景墙、台面 |

## 规格选择

| 空间 | 推荐规格 |
| --- | --- |
| 客厅地面 | 800×800 或 750×1500 |
| 卧室地面 | 600×600 或木纹砖 |
| 厨卫地面 | 300×300 |
| 厨卫墙面 | 300×600 或 400×800 |
| 背景墙 | 750×1500 或岩板 |

## 选购要点

### 看外观

- 表面平整

- 釉面均匀

- 无色差

### 听声音

- 清脆=密度高

- 沉闷=质量差

### 试吸水率

- 地砖≤0.5%

- 墙砖≤10%

### 测防滑性

- 厨卫必须防滑

## 品牌推荐

| 档次 | 品牌 | 价格区间 |
| --- | --- | --- |
| 高端 | 马可波罗、诺贝尔 | 40-100元/片 |
| 中端 | 东鹏、冠珠 | 15-40元/片 |
| 经济 | 地方品牌 | 5-15元/片 |
| 进口 | 蜜蜂、蜘蛛 | 100+元/片 |

## 用量计算

用砖量 = 面积 ÷ 单块面积 × 1.05（5%损耗）
斜铺 × 1.10
人字铺 × 1.15

# 瓷砖选购指南

## 瓷砖分类

| 类型 | 特点 | 适用场景 |
| --- | --- | --- |
| 抛光砖 | 表面光亮、硬度高 | 客厅、餐厅地面 |
| 釉面砖 | 花色丰富、防滑 | 厨卫墙地面 |
| 通体砖 | 正反面一致、耐磨 | 阳台、走廊 |
| 仿古砖 | 复古风格、防滑 | 美式、欧式风格 |
| 木纹砖 | 仿真木地板 | 卧室、客厅 |
| 马赛克 | 装饰性强 | 背景墙、卫浴 |

## 选购要点

### 看外观

- 表面平整无翘曲

- 釉面均匀无色差

- 边角整齐无缺损

### 听声音

- 用硬物敲击，声音清脆说明密度高

- 声音沉闷说明内部有气泡

### 试吸水率

- 在背面滴几滴水

- 吸水慢说明瓷化程度高、质量好

- 地砖吸水率应≤0.5%

### 测防滑性

- 在砖面倒点水，用脚试试

- 厨卫地面必须选防滑砖

## 规格选择

| 空间 | 推荐规格 |
| --- | --- |
| 客厅地面 | 800×800mm 或 600×1200mm |
| 卧室地面 | 600×600mm 或木纹砖 150×900mm |
| 厨卫地面 | 300×300mm 或 400×400mm |
| 厨卫墙面 | 300×600mm |
| 阳台 | 300×300mm 或仿古砖 |

## 用量计算

用砖量 = 铺贴面积 ÷ 单块砖面积 × 1.05（5%损耗）

## 价格参考

| 档次 | 价格区间（元/片） | 代表品牌 |
| --- | --- | --- |
| 低端 | 5-15 | 地方品牌 |
| 中端 | 15-40 | 东鹏、冠珠 |
| 高端 | 40-100 | 马可波罗、诺贝尔 |
| 进口 | 100+ | 蜜蜂、蜘蛛 |

## 铺贴方式

| 方式 | 特点 | 适用风格 |
| --- | --- | --- |
| 直铺 | 整齐规整、省砖 | 现代简约 |
| 斜铺 | 视觉延伸、费砖 | 美式、欧式 |
| 人字铺 | 造型感强、费工 | 法式、北欧 |
| 工字铺 | 错落有致 | 工业风 |

# 墙面材料对比

## 常见墙面材料

| 材料 | 价格（元/㎡） | 寿命 | 特点 |
| --- | --- | --- | --- |
| 乳胶漆 | 20-50 | 5-10年 | 经济、易施工 |
| 壁纸 | 30-200 | 3-8年 | 花色丰富 |
| 壁布 | 50-300 | 5-10年 | 质感好 |
| 硅藻泥 | 100-300 | 10-15年 | 调湿、净化 |
| 艺术涂料 | 80-300 | 10-15年 | 质感丰富 |
| 护墙板 | 200-800 | 15-20年 | 高档、隔音 |
| 瓷砖 | 50-200 | 20年+ | 耐用、易清洁 |

## 乳胶漆

### 优点

- 价格便宜

- 施工简单

- 颜色可选

- 易翻新

### 缺点

- 质感单一

- 易脏

## 壁纸

### 优点

- 花色丰富

- 施工快

- 遮盖墙面缺陷

### 缺点

- 寿命短

- 接缝易翘

- 防潮性差

## 硅藻泥

### 优点

- 调湿

- 净化空气

- 质感好

### 缺点

- 价格高

- 不易清洁

- 颜色选择少

## 选择建议

| 空间 | 推荐材料 |
| --- | --- |
| 客厅 | 乳胶漆/壁布 |
| 卧室 | 乳胶漆/壁纸 |
| 儿童房 | 乳胶漆/硅藻泥 |
| 厨房 | 瓷砖 |
| 卫生间 | 瓷砖 |

# 窗户选购指南

## 窗户类型

| 类型 | 优点 | 缺点 | 适用场景 |
| --- | --- | --- | --- |
| 平开窗 | 密封好 | 占空间 | 卧室、客厅 |
| 推拉窗 | 不占空间 | 密封一般 | 阳台、厨房 |
| 内倒窗 | 通风好 | 价格高 | 卧室 |
| 固定窗 | 采光好 | 不能开 | 客厅大窗 |

## 型材选择

### 断桥铝

| 系列 | 壁厚 | 适用场景 |
| --- | --- | --- |
| 60系列 | 1.4mm | 普通住宅 |
| 70系列 | 1.6mm | 高层住宅 |
| 80系列 | 1.8mm | 别墅 |

## 玻璃选择

| 类型 | 特点 | 适用场景 |
| --- | --- | --- |
| 单层玻璃 | 便宜 | 临时建筑 |
| 双层中空 | 保温隔音 | 住宅推荐 |
| 三层中空 | 保温隔音更好 | 北方 |
| Low-E玻璃 | 隔热好 | 西晒房间 |

## 五金配件

- 选择知名品牌

- 带防坠绳

- 多点锁闭

## 价格参考

| 档次 | 价格（元/㎡） |
| --- | --- |
| 经济 | 300-500 |
| 中档 | 500-800 |
| 高档 | 800-1500 |

## 验收要点

- 型材壁厚达标

- 密封严密

- 开合顺畅

- 3C认证玻璃